## Slide 1: Fabrication of graphitic-carbon suspended nanowires through mechanoelectrospinning of photocrosslinkable polymers
A Osamu Katagiri Tanaka osamu.katagiri@exatec.tec.mx
Assessors:
Héctor Alán Aguirre Soto <alan.aguirre@tec.mx>
Dora Iliana Medina Medina <dora.medina@tec.mx>
30 Jan 2020

## Slide 2: Thesis Overview
Design polymer solutions that can be electrospun by NFES, photopolymerized, and then pyrolyzed into carbon nano-wires.

## Slide 3
in THF & DMF
in THF
No records
in Styrene
in NMP
No records
● FFES
● NFES
Discover a new polymer solution to beat Braulio’s record
Study solutions with high carbon polymers and no oxygen.
SU-8
+
v.s.

## Slide 4
[1] Osswald, T., Rudolph, N., Osswald, T., & Rudolph, N. (2014). Generalized Newtonian Fluid (GNF) Models. Polymer Rheology, 59–99. https://doi.org/10.3139/9781569905234.003
The Carreau-Yasuda Model [1]
zero shear rate viscosity
infinite shear rate viscosity
power law region

## Slide 5
SU-8 +
~4.87 μm diameter fibers [2]
~4.68 μm diameter fibers [2]
~4.35 μm diameter fibers [2]
~1.58 μm diameter fibers [2]
no successful depositions of pure SU-8 [2]
Flores, D. R. (2017). Role of rheological properties in near field electrospun fibers morphology, 130.

## Slide 9: Q&A

## Slide 13: Characterization of the 0.25 wt% PEO Solution
Electrospun-able with an applied voltage of 600V.
600V
700V
Unable to initiate the jet at 500V or lower.
Notes: Surface t-

## Slide 16: PEO Solution
The EMS polymer solution consisted of
2ml of SU-8 2002 mixed with
0.5 wt% of Poly(ethylene oxide) (PEO, 4,000,000 MW; SigmaAldrich Inc., Cat. N. 189464) and
0.5 wt% Tetrabutylammonium Tetrafluoroborate salts (TBATFB; SigmaAldrich Inc., Cat. N. 217964) to increase its conductivity and allow smooth polymer flow during electrospinning.
All reagents were used as received. Magnetic stirring of these components was performed for 1hr at 75°C and low rpm (100-150 rpm).

## Slide 17
https://www.fishersci.com/shop/products/NC0702370/nc0702370#?keyword=MICROCHEM+CORP+PHOTORESIST+SU-8
https://www.fishersci.com/shop/products/NC9901158/nc9901158#?keyword=SU-8++developer
Notes: https://rsc.aux.eng.ufl.edu/_files/msds/309.pdf

## Slide 18: Zero shear viscosity measurements and Flores’ measurements
Both measurements have the same behaviour with similar proportions.
However, the results show that the current measured values are approximately three times larger than Flores’ measurements.

## Slide 19: <subTitle>
<content> <key concept>