## Slide 1: Fabrication of graphitic-carbon suspended nanowires through mechano-electrospinning of photo-crosslinkable polymers
Osamu Katagiri-Tanaka A01212611@itesm.mx
Principal Advisor: Dr. Héctor Alán Aguirre Soto Co-advisor and Director of Program: Dra. Dora Iliana Medina Medina
25 Nov 2020

## Slide 2: Agenda
Motivation & Problem Statement : 10 min
Objectives : 3 min
NFES literature review : 10 min
Rheology Analyses : 10 min
Fabrication & Characterization : 5 min
Future Work : 3 min

## Slide 3: Motivation & Problem Statement

## Slide 4: Carbon Based Nanomaterials (CBNs)
R.L. McCreery, Advanced Carbon Electrode Materials for Molecular Electrochemistry, Chem. Rev. 108 (2008) 2646–2687. https://doi.org/10.1021/cr068076m.
S. Beigi-boroujeni, O. Katagiri-tanaka, B. Cardenas-benitez, O. Sergio, A. Aguirre-soto, Pyrolytic Carbon from Novolac Epoxy Resin Compressed before Photocrosslinking and Pyrolysis, Mater. Today Proc. (2020).
The crystallite size, molecular arrangement, and anisotropy determine the material’s properties.
The interminable collection of CBNs range from soft, conductive lubricants to very hard, low conductivity solids; and from black colour, bulks to transparent, disordered thin films
Notes: * Classification in a diagram with ranges and units (characterization techniques)

## Slide 5: Carbon allotropes
R.B. Heimann, S.E. Evsvukov, Y. Koga, Carbon allotropes: a suggested classification scheme based on valence orbital hybridization, Carbon N. Y. 35 (1997) 1654–1658. https://doi.org/10.1016/S0008-6223(97)82794-7.
Е.А. Belenkov, Classification of carbon structures, in: Carbon Nanotub. Graphene, Chelyabinsk State University, Chelyabinsk, Russia, 2003: p. 5.
M. Fedel, Blood compatibility of diamond-like carbon (DLC) coatings, in: Diamond-Based Mater. Biomed. Appl., Elsevier, 2013: pp. 71–102. https://doi.org/10.1533/9780857093516.1.71.
M. Razeghi, Fundamentals of Solid State Engineering, Springer International Publishing, Cham, 2019. https://doi.org/10.1007/978-3-319-75708-7.
K. Alstrup Jensen, J. Bøgelund, P. Jackson, N. Raun Jacobsen, R. Birkedal, P. Axel Clausen, A. Thoustrup Saber, H. Wallin, U. Birgitte Vogel, Carbon nanotubes - Types, products, market, and provisional assessment of the associated risks to man and the environment, The Danish Environmental Protection Agency, 2015.

## Slide 6: Carbon allotropes
R.L. McCreery, Advanced Carbon Electrode Materials for Molecular Electrochemistry, Chem. Rev. 108 (2008) 2646–2687. https://doi.org/10.1021/cr068076m.
S. Beigi-boroujeni, O. Katagiri-tanaka, B. Cardenas-benitez, O. Sergio, A. Aguirre-soto, Pyrolytic Carbon from Novolac Epoxy Resin Compressed before Photocrosslinking and Pyrolysis, Mater. Today Proc. (2020).
Harry Marsh. Introduction to Carbon Science. Vol. 46. 1. Elsevier, Apr. 1989, p. 43. ISBN: 9780408038379. DOI: 10.1016/C2013- 0- 04111- 4. URL: https: //linkinghub.elsevier.com/retrieve/pii/C20130041114.
Pierson Hugh. Handbook of Carbon, Graphite, Diamonds and Fullerenes. Elsevier, 1994, p. 419. ISBN: 9780815513391.
Notes: Add Triangle diagram
Focus in GLC

## Slide 7: Glass-like Carbon
R.L. McCreery, Advanced Carbon Electrode Materials for Molecular Electrochemistry, Chem. Rev. 108 (2008) 2646–2687. https://doi.org/10.1021/cr068076m.
G. Speranza, The Role of Functionalization in the Applications of Carbon Materials: An Overview, C — J. Carbon Res. 5 (2019) 84. https://doi.org/10.3390/c5040084.
Attractive for its electrochemical stability, thermal resistance, electrical conductivity, biocompatibility and is gas impermeable.
It is used in the manufacture of semiconductors.

## Slide 8: MicroChem’s SU-8 & Tokai’s recipe
R.L. McCreery, Advanced Carbon Electrode Materials for Molecular Electrochemistry, Chem. Rev. 108 (2008) 2646–2687. https://doi.org/10.1021/cr068076m.
G. Speranza, The Role of Functionalization in the Applications of Carbon Materials: An Overview, C — J. Carbon Res. 5 (2019) 84. https://doi.org/10.3390/c5040084.
Electrical resistivity, comparison:
highly oriented pyrolytic graphite (HOPG)
SU-8 glass-like carbon
TOKAI Glassy carbon
<
x103
<
x4
Tokai’s recipe is a secret …
Notes: * Focus in microchem

## Slide 9: MicroChem’s SU-8 & Tokai’s recipe
<content> <key concept>
R.L. McCreery, Advanced Carbon Electrode Materials for Molecular Electrochemistry, Chem. Rev. 108 (2008) 2646–2687. https://doi.org/10.1021/cr068076m.
G. Speranza, The Role of Functionalization in the Applications of Carbon Materials: An Overview, C — J. Carbon Res. 5 (2019) 84. https://doi.org/10.3390/c5040084.
SU-8
glass-like carbon resistivity:

## Slide 10: Current approaches
V. Galstyan, M. Bhandari, V. Sberveglieri, G. Sberveglieri, E. Comini, Metal Oxide Nanostructures in Food Applications: Quality Control and Packaging, Chemosensors. 6 (2018) 16. https://doi.org/10.3390/chemosensors6020016.
D. Kluge, J.C. Singer, B.R. Neugirg, J.W. Neubauer, H.-W. Schmidt, A. Fery, Top–down meets bottom–up: A comparison of the mechanical properties of melt electrospun and self-assembled 1,3,5-benzenetrisamide fibers, Polymer (Guildf). 53 (2012) 5754–5759. https://doi.org/10.1016/j.polymer.2012.10.016.
Photolithography
Physical & Optical Limitations
Two-Photon Polymerization (TPP)
Slow (mm per sec) & Expensive
*Near-Field Electrospinning (NFES)
Suspended Nanowires w/Spatial Control

## Slide 11: Glass-like Carbon NWs: Applications
V. Baudrit J, Recycling and Elimination of Wastes obtained from Agriculture by using Nanotechnology: Nanosensors, Int. J. Biosens. Bioelectron. 3 (2017) 368–375.https://doi.org/10.15406/ijbsbe.2017.03.00084.
R.L. McCreery, Advanced Carbon Electrode Materials for Molecular Electrochemistry, Chem. Rev. 108 (2008) 2646–2687. https://doi.org/10.1021/cr068076m.
G. Speranza, The Role of Functionalization in the Applications of Carbon Materials: An Overview, C — J. Carbon Res. 5 (2019) 84. https://doi.org/10.3390/c5040084.
Notes: Remove general words (Applocations -> detection/sensors)
Problemas que solucionan estos sensores (contaminantes en agua, aire, temperatura en electrónicos, health care)

## Slide 12: MicroChem’s SU-8
However, photolithography generates waste in the spin-coating and developing steps. Also, it presents structural limitations.
Microchem, Su-8 2000.5-2015, 2000.5, 2002, 2005, 2007, 2010, 2015. (2006) 1–5. papers3://publication/uuid/859F51B9-0382-4DE8-88A9-267F936939A3.
Pyrolysis of SU8 is currently the typical method to produce glass-like carbon.
Polymer patterning through photolithography
Carbonization through pyrolysis
Limitations can be overcome with other fabrication techniques, such as NFES

## Slide 13: MicroChem’s SU-8
To provided the required viscosity
To increase the solution conductivity
… both needed for smooth PEO flow during electrospinning
SU-8 + TBF + PEO
However, SU-8 as is not electrospinnable
SU-8 does not have the right viscosity & solution conductivity.
SU-8 is design for photolithography.
D.R. Flores, Role of rheological properties in near field electrospun fibers morphology, (2017) 130.
B. Cárdenas Benítez, Advanced Manufacturing Techniques for the Fabrication and Surface Modification of Carbon Nanowires, Tecnológico de Monterrey, 2017.
Notes: Remove background from figures
Para las aplicationes necesito que sea electrospinnalbe
Photolithography-able vs. Electrospinnableility
Highlight the PEO

## Slide 14: NFES Process Parameters
The interdependence between the process and solution parameters presents a challenge to predict the fiber morphology.
Properties of an electrospun fiber depend on many parameters,
and each parameter also depends on the polymer-solvent system.
S.B. Gadkari, Scaling analysis for electrospinning, Springerplus. 3 (2014) 705. https://doi.org/10.1186/2193-1801-3-705.
Solution Parameters:
Concentration
Molecular weight
Viscosity
Electrical conductivity
Ambient Parameters:
Humidity
Temperature
Process Parameters:
Applied Voltage
Flow rate
Working distance
Notes: Predicción de diámetro y control espacial
Mention my important parameters: conductivity low diameter spatial control
Challenge de control de diametro

## Slide 15: Best Results so far by NFES (previous work)
Fiber yield rate of 81 %
Fiber diameter before pyrolysis of 4.966 μm
Fiber diameter after pyrolysis of 204 nm
Fiber length of 60.5 ± 4.3 μm
Fiber resistance from 407 KΩ to 1.727 MΩ
wt% PEO 0.25 | SU-8 2002 [mg] | PEO [mg] | TBF [mg]
 | 2246 | 5.65 | 11.32
D.R. Flores, Role of rheological properties in near field electrospun fibers morphology, (2017) 130.
B. Cárdenas Benítez, Advanced Manufacturing Techniques for the Fabrication and Surface Modification of Carbon Nanowires, Tecnológico de Monterrey, 2017.

## Slide 16: Methods: Implications of PEO
The fiber yield rate and fiber conductivity are impacted negatively as PEO introduces more oxygen to the solution
The addition of oxygen decreases the char yield.
High variance in the obtained conductivity across samples.
Some samples are destroyed during pyrolysis
D.R. Flores, Role of rheological properties in near field electrospun fibers morphology, (2017) 130.
B. Cárdenas Benítez, Advanced Manufacturing Techniques for the Fabrication and Surface Modification of Carbon Nanowires, Tecnológico de Monterrey, 2017.
Notes: Diagram – PEO pyrolysis
Mention the rol of Oxygen – abd connect it witht the desired characteristics – closed porous
Pyrolysis stages
Balance of properties

## Slide 17: Objectives

## Slide 18: Objectives
General. Formulate polymer/solvent combinations that have the greatest potential to replace or modify the SU-8/PEO formulation for the fabrication of microscopic polymer fibers that may be converted to conductive suspended carbon nano- wires.
Specific1. Learn how the diameter of the electrospun polymer fiber can be controlled by appropriate tuning of the NFES parameters and solution properties.
Specific2. Through rheological analyses, determine if polymer solutions have comparative viscoelastic properties to those of the SU- 8/PEO benchmark, and if they can be easily electrospun by NFES.
Specific3. Propose alternatives to the SU-8/PEO benchmark formulation for the production of microscopic polymer fibers with potential for the fabrication of carbon nano-wires.

## Slide 19: NFES literature review
Specific Objective 1. Learn how the diameter of the electrospun polymer fiber can be controlled by appropriate tuning of the NFES parameters and solution properties.
Notes: To find substitutions to keep
Spatial control, high conductivity, low diameter
Find new formulations or replace PEO in SU8 -> find new materials

## Slide 20: Methods: NFES literature (first NFES apparatus built in 2003 by J. Kameoka et al.)
J. Kameoka, R. Orth, Y. Yang, D. Czaplewski, R. Mathers, G.W. Coates, H.G. Craighead, A scanning tip electrospinning source for deposition of oriented nanofibres, Nanotechnology. 14 (2003) 1124–1129. https://doi.org/10.1088/0957-4484/14/10/310.
C. Chang, K. Limkrailassiri, L. Lin, Continuous near-field electrospinning for large area deposition of orderly nanofiber patterns, Appl Phys Lett. (2008) 3. https://doi.org/10.1063/1.2975834.
Thinnest fiber achieved by C. Chang et al. with ~50 nm in diameter. (PEO in water)
However, fiber yield rate was not reported

## Slide 21: Methods: Data collection (analysis of NFES articles from 2003 to 2020)
The author mentions the process parameters and fiber properties within the article in writing.
Figures from Min2013
Fattahi2017
S.-Y. Min, T.-S. Kim, B.J. Kim, H. Cho, Y.-Y. Noh, H. Yang, J.H. Cho, T.-W. Lee, Large-scale organic nanowire lithography and electronics, Nat. Commun. 4 (2013) 1773. https://doi.org/10.1038/ncomms2785.
P. Fattahi, J.T. Dover, J.L. Brown, 3D Near-Field Electrospinning of Biomaterial Microfibers with Potential for Blended Microfiber-Cell-Loaded Gel Composite Structures, Adv. Healthc. Mater. 6 (2017) 1700456. https://doi.org/10.1002/adhm.201700456.

## Slide 22: Methods: Data collection (analysis of NFES articles from 2003 to 2020)
The author provides the data in plots and graphs.
WebPlotDigitalizer (https://github.com/ankitrohatgi/WebPlotDigitizer):
Applied voltage vs. fiber diameter by Madou2011
M.J. Madou, D. Dunn-Rankin, L. Kulinsky, A. Mirsepassi, G.S. Bisht, S. Oh, G. Canton, Controlled Continuous Patterning of Polymeric Nanofibers on Three-Dimensional Substrates Using Low-Voltage Near-Field Electrospinning, Nano Lett. 11 (2011) 1831–1837. https://doi.org/10.1021/nl2006164.

## Slide 23: Methods: Data collection (analysis of NFES articles from 2003 to 2020)
The author does not mention the fiber diameter in writing but provides a EM characterization.
Python Image Analysis (with a 3.2% error in avg.):
Figures from Camillo2013
Figures from Min2013
S.-Y. Min, T.-S. Kim, B.J. Kim, H. Cho, Y.-Y. Noh, H. Yang, J.H. Cho, T.-W. Lee, Large-scale organic nanowire lithography and electronics, Nat. Commun. 4 (2013) 1773. https://doi.org/10.1038/ncomms2785..
https://github.com/katagirimx/OpenCV-image-measuring
D. Di Camillo, V. Fasano, F. Ruggieri, S. Santucci, L. Lozzi, A. Camposeo, D. Pisignano, Near-field electrospinning of conjugated polymer light-emitting nanofibers, Nanoscale. 5 (2013) 11637–11642. https://doi.org/10.1039/C3NR03094F.

## Slide 24: Conclusion 1.1:
Polymer Concentration,
Nozzle Diameter,
Solution Flow Rate,
Working Distance,
&
Applied Voltage
are the main drivers of the final Fiber Diameter

## Slide 25
low polymer
concentrations
slow solution flow rates
small needle
diameters
low voltages
25
Conclusion 1.1:
Process Parameters

## Slide 26: Conclusion 1.2: Let’s focus on polymer concentration
Polymer concentration is the most reliable process parameter to control the morphology of electrospun fibers. (regardless the type of NFES process)

## Slide 27: Conclusion 1.2: Let’s focus on polymer concentration
Polymer concentration is the most reliable process parameter to control the morphology of electrospun fibers. (regardless the type of NFES process)
Notes: Song2015 : glass capillary tip
Brown201X : melt ES
Husain2016 : L = cm
Shin2019 : coiled/meander fibers
Parajuli2016 : concentrations 25 – 80%

## Slide 28: Diameter Prediction of Electrospun Fibers
N. Liu, K. Kim, H.Y. Jeong, P.C. Hsu, Y. Cui, Z. Bao, Effect of Chemical Structure on Polymer-Templated Growth of Graphitic Nanoribbons, ACS Nano. 9 (2015) 9043–9049. https://doi.org/10.1021/acsnano.5b03134.

## Slide 29: Diameter Prediction of Electrospun Fibers
N. Liu, K. Kim, H.Y. Jeong, P.C. Hsu, Y. Cui, Z. Bao, Effect of Chemical Structure on Polymer-Templated Growth of Graphitic Nanoribbons, ACS Nano. 9 (2015) 9043–9049. https://doi.org/10.1021/acsnano.5b03134.

## Slide 30: Diameter Prediction of Electrospun Fibers
N. Liu, K. Kim, H.Y. Jeong, P.C. Hsu, Y. Cui, Z. Bao, Effect of Chemical Structure on Polymer-Templated Growth of Graphitic Nanoribbons, ACS Nano. 9 (2015) 9043–9049. https://doi.org/10.1021/acsnano.5b03134.

## Slide 31: Conclusion1.3: Selection of Polymer-Solvent combinations
N. Liu, K. Kim, H.Y. Jeong, P.C. Hsu, Y. Cui, Z. Bao, Effect of Chemical Structure on Polymer-Templated Growth of Graphitic Nanoribbons, ACS Nano. 9 (2015) 9043–9049. https://doi.org/10.1021/acsnano.5b03134.
higher sp2 carbon content translates into higher graphitization degree and higher electrical conductivity
polymers with functional groups are required for the creation of smooth and continuous fibers.
Zhenan Bao et al. investigated the effect of the polymer chemical
Structure of:
Notes: Bao lit review
Mention templating effect & pipeline stacking
PVP and Novolac have one benzene ring in each repeating unit,
PVA is mainly made out of sp3 carbon
PS is not functionalized

## Slide 32: Conclusion1.3: Selection of Polymer-Solvent combinations
Polymers with high carbon content relative to oxygen content
A.A. Yousefi, A.R. Mohebbi, S. Falahdoost Moghadam, S.A. Poursamar, L. Hao, Uniaxially aligned microwire networks for flexible transparent electrodes using a novel electrospinning set-up, Sol. Energy. 188 (2019) 1111–1117. ttps://doi.org/10.1016/j.solener.2019.07.007.
H. Fong, D.H. Reneker, Elastomeric nanofibers of styrene-butadiene-styrene triblock copolymer, J. Polym. Sci. Part B Polym. Phys. 37 (1999) 3488–3493. https://doi.org/10.1002/(SICI)1099-0488(19991215)37:24<3488::AID-POLB9>3.0.CO;2-M.
S.-Y. Min, T.-S. Kim, B.J. Kim, H. Cho, Y.-Y. Noh, H. Yang, J.H. Cho, T.-W. Lee, Large-scale organic nanowire lithography and electronics, Nat. Commun. 4 (2013) 1773. https://doi.org/10.1038/ncomms2785.
Notes: Mw
Aromaticidad
Cantidad de carbono
Ratio oxygen / carbon in pyrolysis

## Slide 33: Rheology Analyses
Specific Objective 2. Through rheological analyses, determine if polymer solutions have comparative viscoelastic properties to those of the SU-8/PEO benchmark, and if they can be easily electrospun by NFES.

## Slide 34
Under some critical concentration NFES yields beads or small fibres
Over some critical concentration NFES continuous fibres
Viscosity increases with molecular weight
The general belief is that the molecular weight needs to be sufficient enough to create or induce entanglements
D.R. Flores, Role of rheological properties in near field electrospun fibers morphology, (2017) 130.
G.L. Wilkes, An overview of the basic rheological behavior of polymer fluids with an emphasis on polymer melts, J. Chem. Educ. 58 (1981) 880. https://doi.org/10.1021/ed058p880.
Literature claims

## Slide 35
As “electropinnability” is determined by the polymer chain entanglement,
chain entanglement is controlled by molecular weight,
increasing molecular weight increases viscosity, and
viscosity is controlled by polymer concentration, then
The critical/spinnable concentration can be found in a viscosity vs. concentration plot
critical
concentration
Literature claims
D.R. Flores, Role of rheological properties in near field electrospun fibers morphology, (2017) 130.
G.L. Wilkes, An overview of the basic rheological behavior of polymer fluids with an emphasis on polymer melts, J. Chem. Educ. 58 (1981) 880. https://doi.org/10.1021/ed058p880.

## Slide 36: Methods: Sample Preparation (SU8-PEO)
3.0 ml samples
on a heating plate at 160 rpm and 60°C, for 2 hours each

## Slide 37: Methods: Sample Preparation (PS & PSB)

## Slide 38: Methods: Sample Preparation (PSB & PSMS)

## Slide 39: Methods: Sample Preparation (PVK & SU8-PVK)

## Slide 40: Methods: Rheology – Frequency Sweeps
Geometry:
Steel cone plate, Peltier plate
(60.0 mm diameter, 0.9979° cone angle, 23 µm truncation)
Procedure:
Frequency sweep
(20°C, for 20 min
from to 1/s shear rates)

## Slide 41
Methods: The Carreau-Yasuda Model
: viscosity
: shear rate
: infinite shear rate viscosity
: zero shear rate viscosity
: time constant
: Power Law index
: width of the transition region

## Slide 42
Methods: Other models:

## Slide 43
Methods: Other models:

## Slide 44
Methods: Rheology results validation for 0wt% PEO
MicroChem data sheet:
Measured:
Microchem, Su-8 2000.5, 2002, 2005, 2007, 2010, 2015, Microchem. (2018) 1–5. papers3://publication/uuid/859F51B9-0382-4DE8-88A9-267F936939A3.
vs.
from PEO in SU8 sample set
from PVK in SU8 sample set

## Slide 45
Methods: Rheology results validation for 0wt% PEO
Anton-Paar data sheet:
Measured:
https://wiki.anton-paar.com/en/chloroform/
vs.

## Slide 46
D.R. Flores, Role of rheological properties in near field electrospun fibers morphology, (2017) 130.
Notes: D.R. Flores, Role of rheological properties in near field electrospun fibers morphology, (2017) 130.

## Slide 47
Methods: Rheology results validation
D.R. Flores-hernandez, B. Cardenas-benitez, S.O. Martinez-chapa, J. Bonilla-rios, Tailoring the Diameters of Electro-Mechanically Spun Fibers by Controlling Their Deborah Numbers, (2020). https://doi.org/10.3390/polym12061358.
Notes: D.R. Flores-hernandez, B. Cardenas-benitez, S.O. Martinez-chapa, J. Bonilla-rios, Tailoring the Diameters of Electro-Mechanically Spun Fibers by Controlling Their Deborah Numbers, (2020). https://doi.org/10.3390/polym12061358.

## Slide 48
Methods: Rheology results validation
G.S. Bisht, G. Canton, A. Mirsepassi, L. Kulinsky, S. Oh, D. Dunn-Rankin, M.J. Madou, D. Dunn-Rankin, L. Kulinsky, A. Mirsepassi, G.S. Bisht, S. Oh, G. Canton, Controlled Continuous Patterning of Polymeric Nanofibers on Three-Dimensional Substrates Using Low-Voltage Near-Field Electrospinning, Nano Lett. 11 (2011) 1831–1837. https://doi.org/10.1021/nl2006164.
Notes: D.R. Flores-hernandez, B. Cardenas-benitez, S.O. Martinez-chapa, J. Bonilla-rios, Tailoring the Diameters of Electro-Mechanically Spun Fibers by Controlling Their Deborah Numbers, (2020). https://doi.org/10.3390/polym12061358.

## Slide 49
spinnable
concentrations
non-spinnable concentrations
c*=25 wt%
Spinnable/Critical Concentration

## Slide 50
Spinnable/Critical Concentration

## Slide 51
Spinnable/Critical Concentration
Vu Anh Doan et al. “Interphase transfer of tackifier between poly(butadiene) and poly(styrene-co-butadiene)”. In: Journal of Materials Science 48.5 (Mar. 2013), pp. 2046–2052. ISSN: 0022-2461. DOI: 10.1007/s10853- 012- 6974- 1. URL: http://link.springer.com/10.1007/s10853-012-6974-1.
Ralph H. Colby, Lewis J. Fetters, and William W. Graessley. “The melt viscosity-molecular weight relationship for linear polymers”. In: Macromolecules 20.9 (Sept. 1987), pp. 2226–2237. ISSN: 0024-9297. DOI: 10 . 1021 / ma00175a030. URL: https : / / pubs . acs . org / doi / abs / 10 . 1021 / ma00175a030.

## Slide 52
POLYSTYRENE
TETRAHYDROFURAN
c*

## Slide 53
POLY(STYRENE-CO-BUTADIENE)
1-METHYL-2-PYRROLIDINONE
c*

## Slide 54
POLY(STYRENE-CO-BUTADIENE)
75% TETRAHYDROFURAN / 25% N,N-DIMETHYLFORMAMIDE
c*

## Slide 55
POLY(STYRENE-CO-ALPHA-METHYLSTYRENE)
N,N-DIMETHYLFORMAMIDE
c*

## Slide 56
POLY(9-VINYLCARBAZOLE)
CHLOROFORM

## Slide 57
POLY(9-VINYLCARBAZOLE)
DICHLOROMETHANE

## Slide 58: Conclusion2.1: Polymer-Solvent concentrations
Polymer / Solvent | Critical / spinnable concentration | Molecular Weight
Poly(Ethylene Oxide) / SU-8 Cyclopentanone | 0.25 wt% | 4 000 000
Polystyrene Tetrahydrofuran | 15.17 wt% | 192 000
Poly(Styrene-co-Butadiene) 1-Methyl-2-Pyrrolidinone | 7.74 wt% | 
Poly(Styrene-co-Butadiene) 75% THF / 25% DMF | 13.75 wt% | 
Poly(Styrene-co-α-Methylstyrene) N,N-Dimethylformamide | 4.94 wt% | 
Poly(9-Vinylcarbazole) Chloroform | 0.75 wt% | 1 100 000
Poly(9-Vinylcarbazole) / SU-8 Cyclopentanone | 15.0 wt% | 1 100 000
Notes: Note Mw of each polymer

## Slide 59: Fabrication & Characterization
Specific Objective 3. Propose alternatives to the SU-8/PEO benchmark formulation for the production of microscopic polymer fibers with potential for the fabrication of carbon nano-wires.

## Slide 60
Methods: Design of experiments / NFES
Given the results of previous work, the experiments shall reflect:
The SU8-PEO sample set is the control
The critical concentration will be used for each sample set
  Other process parameters (working distance, stage velocity, flow rate) are to be tuned and remain constant during NFES.

## Slide 61: Conclusion3.1: spinnable solutions
Polymer / Solvent | Critical / spinnable concentration
Poly(Ethylene Oxide) SU-8 | 0.25 wt%
Polystyrene Tetrahydrofuran | 15.17 wt%
Poly(Styrene-co-Butadiene) 75% THF / 25% DMF | 13.75 wt%
Poly(9-vinylcarbazole) Chloroform | (15.00 wt%)
Fabrication velocity: 1000um
Acceleration: 500mm/s^2
Working distance: 1500um
Applied voltage: 600V
Applied current: 15uA
Deposition rate: 0.3uL/min
Spacing: 10um

## Slide 62: Conclusion3.1: non-spinnable solutions
Polymer / Solvent | Critical / spinnable concentration | rationale
Poly(Styrene-co-α-Methylstyrene) N,N-Dimethylformamide | 4.94 wt% | Fibres were broken into agglomerates / dust
Poly(9-vinylcarbazole) Dichloromethane | (15.00 wt%) | Fast volatilization, creating a Shell around the drop.
Notes: Poly(Styrene-co-Butadiene)
1-Methyl-2-Pyrrolidinone
7.74 wt%

## Slide 63: Next Steps < work pending >

## Slide 64
Prediction of Fibre diameter and characterization of fibres
vs.

## Slide 67: SU-8 (MicroChem, US)
Notes: https://rsc.aux.eng.ufl.edu/_files/msds/309.pdf

## Slide 68: Carbon nanostructures via Lithography
The production of C-MEMS:
Polymer patterning through photolithography electrospinning
Carbonization through pyrolysis
● SU-8 Waste
● Physical & Optical Limitations
● Structure Limitations
photolithography process

## Slide 69: TPP – Two-Photon Polymerization
B. Cardenas-Benitez, C. Eschenbaum, D. Mager, J.G. Korvink, M.J. Madou, U. Lemmer, I. De Leon, S.O. Martinez-Chapa, Pyrolysis-induced shrinking of three-dimensional structures fabricated by two-photon polymerization: experiment and theoretical model, Microsystems Nanoeng. 5 (2019). https://doi.org/10.1038/s41378-019-0079-9.

## Slide 70: Characterization of the 0.25 wt% PEO Solution
Notes: Surface t-

## Slide 72
wt% in THF & DMF
wt% in THF
wt% in DMF
wt% in CHL
wt% in NMP
wt% in DCM

## Slide 74: Characterization of the 0.25 wt% PEO Solution
Electrospun-able with an applied voltage of 600V.
600V
700V
Unable to initiate the jet at 200V or lower.
Notes: Surface t-

## Slide 77: SU-8 (MicroChem, US)
https://www.fishersci.com/shop/products/NC0702370/nc0702370#?keyword=MICROCHEM+CORP+PHOTORESIST+SU-8
https://www.fishersci.com/shop/products/NC9901158/nc9901158#?keyword=SU-8++developer
Notes: https://rsc.aux.eng.ufl.edu/_files/msds/309.pdf

## Slide 78: Materials

## Slide 79: title:
<content> <key concept> <key concept>
<a point>
<another point>
D.R. Flores-hernandez, B. Cardenas-benitez, S.O. Martinez-chapa, J. Bonilla-rios, Tailoring the Diameters of Electro-Mechanically Spun Fibers by Controlling Their Deborah Numbers, (2020). https://doi.org/10.3390/polym12061358.