## Slide 1: Fabrication of graphitic-carbon suspended nanowires through mechano-electrospinning of photocrosslinkable polymers
A Osamu Katagiri Tanaka A01212611@itesm.mx
08 Apr 2020

## Slide 2: Motivation & Problem Statement

## Slide 3: Current approaches for the fabrication of carbon nanowires (CNWs)
V. Galstyan, M. Bhandari, V. Sberveglieri, G. Sberveglieri, E. Comini, Metal Oxide Nanostructures in Food Applications: Quality Control and Packaging, Chemosensors. 6 (2018) 16. https://doi.org/10.3390/chemosensors6020016.
D. Kluge, J.C. Singer, B.R. Neugirg, J.W. Neubauer, H.-W. Schmidt, A. Fery, Top–down meets bottom–up: A comparison of the mechanical properties of melt electrospun and self-assembled 1,3,5-benzenetrisamide fibers, Polymer (Guildf). 53 (2012) 5754–5759. https://doi.org/10.1016/j.polymer.2012.10.016.
Lithography
Physical & Optical Limitations
Near-Field Electrospinning (NFES)
Can fabricate Suspended Nanowires w/Spatial Control
Self-assembly
Limited Length and Random Orientation
Two-Photon Polymerization (TPP)
Slow (mm per sec) & Expensive

## Slide 4: Thesis Overview
Design polymer solutions that can be electrospun by NFES, photopolymerized, and then pyrolyzed into conductive carbon nano-wires.

## Slide 5: Polymer Solution Parameters

## Slide 6: SU-8 Carbon Structures
The production of C-MEMS:
Polymer patterning through photolithography
Carbonization through pyrolysis
However, SU-8 as is can not electrospin
SU-8 does not have the right viscosity & solution conductivity
SU-8 is design for photolithography
Microchem, Su-8 2000.5-2015, 2000.5, 2002, 2005, 2007, 2010, 2015. (2006) 1–5. papers3://publication/uuid/859F51B9-0382-4DE8-88A9-267F936939A3.

## Slide 7: Making SU-8 spunable (by Braulio & Ricardo)
To provided the required viscosity
To increase the solution conductivity
… both needed for smooth PEO flow during electrospinning
SU-8 + TBF + PEO
B. Cárdenas, Advanced Manufacturing Techniques for the Fabrication and Surface Modification of Carbon Nanowires, (2017) 160.
D.R. Flores, Role of rheological properties in near field electrospun fibers morphology, (2017) 130.
Notes: Surface t-

## Slide 8: Results with amended SU-8
The modified solution is spunable
Fiber diameter before pyrolysis of 4.966 μm
Fiber diameter after pyrolysis of 204 nm
But, somewhat pyrolyzable
Fiber resistivity from 407 KΩ to 1.727 MΩ
Fiber yield rate of 81 %
wt% PEO 0.25 | SU-8 2002 [mg] | PEO [mg] | TBT [mg]
 | 2246 | 5.65 | 11.32
= 2 ml of solution
Achieved with:

## Slide 9: Implications of PEO, as it introduces oxygen to the solution
The fiber yield rate and fiber conductivity are impacted negatively.
In the presence of oxygen, the char yield decreases. This is due to the oxidation on the char.
High variance in the obtained conductivity across samples.
Some samples are destroyed during pyrolysis
Notes: Surface t-

## Slide 10: Rheology of the amended SU-8 solution (0.25 wt%)
The 0.25 wt% sample (orange line) has a zero-shear viscosity (ZSV) of 60 Pa.s
Let’s discover new polymer solutions with similar rheology (and no oxygen)

## Slide 11
25 wt% in THF & DMF
35 wt% in THF
15 wt% in DMF
8 wt% in CHL
15 wt% in NMP
7 wt% in DCM

## Slide 12: NFES Process Parameters

## Slide 13: Data collection from 30+ NFES papers
Python Image Analysis
WebPlotDigitalizer https://github.com/ankitrohatgi/WebPlotDigitizer
Applied voltage vs. fiber diameter by Madou2011
Figure from Camillo2013
Figure from Min2013

## Slide 14
Polymer Concentration,
Nozzle Diameter,
Solution Deposition Rate,
Nozzle to Collector Distance &
Applied Voltage
are the main drivers of the final Fiber Diameter

## Slide 15
low polymer concentrations
slow solution deposition rates
short nozzle to collector distances
low voltages

## Slide 16: Overall Progress & Next Steps

## Slide 17: Current Work Plan
today
rheology

## Slide 18
~15 wt% in NMP
~25 wt% in THF & DMF
+35 wt% in THF
+15 wt% in DMF
~8 wt% in CHL
No records
No records
Next step: Study/Test the proposed polymer solutions
high carbon polymers and no oxygen

## Slide 20: Carbon nanostructures via Lithography
The production of C-MEMS:
Polymer patterning through photolithography electrospinning
Carbonization through pyrolysis
● SU-8 Waste
● Physical & Optical Limitations
● Structure Limitations
photolithography process

## Slide 21: TPP – Two-Photon Polymerization
B. Cardenas-Benitez, C. Eschenbaum, D. Mager, J.G. Korvink, M.J. Madou, U. Lemmer, I. De Leon, S.O. Martinez-Chapa, Pyrolysis-induced shrinking of three-dimensional structures fabricated by two-photon polymerization: experiment and theoretical model, Microsystems Nanoeng. 5 (2019). https://doi.org/10.1038/s41378-019-0079-9.

## Slide 22: Characterization of the 0.25 wt% PEO Solution
Notes: Surface t-

## Slide 23: Characterization of the 0.25 wt% PEO Solution
Electrospun-able with an applied voltage of 600V.
600V
700V
Unable to initiate the jet at 500V or lower.
Notes: Surface t-

## Slide 26: PEO Solution
The EMS polymer solution consisted of
2ml of SU-8 2002 mixed with
0.5 wt% of Poly(ethylene oxide) (PEO, 4,000,000 MW; SigmaAldrich Inc., Cat. N. 189464) and
0.5 wt% Tetrabutylammonium Tetrafluoroborate salts (TBATFB; SigmaAldrich Inc., Cat. N. 217964) to increase its conductivity and allow smooth polymer flow during electrospinning.
All reagents were used as received. Magnetic stirring of these components was performed for 1hr at 75°C and low rpm (100-150 rpm).

## Slide 27: Applications of CNWs

## Slide 28: SU-8 (MicroChem,US)
Notes: https://rsc.aux.eng.ufl.edu/_files/msds/309.pdf

## Slide 29: SU-8 (MicroChem, US)
https://www.fishersci.com/shop/products/NC0702370/nc0702370#?keyword=MICROCHEM+CORP+PHOTORESIST+SU-8
https://www.fishersci.com/shop/products/NC9901158/nc9901158#?keyword=SU-8++developer
Notes: https://rsc.aux.eng.ufl.edu/_files/msds/309.pdf

## Slide 30: <subTitle>
<content> <key concept>