## Slide 1: Fabrication of graphitic-carbon suspended nanowires through mechano-electrospinning of photocrosslinkable polymers
Osamu Katagiri-Tanaka A01212611@itesm.mx
Principal Advisor: Dr. Héctor Alán Aguirre Soto Co-advisor and Director of Program: Dra. Dora Iliana Medina Medina
15 May 2020

## Slide 2: Agenda
<a point for discussion> : <5min
<another point for discussion> : ~20min

## Slide 3: Motivation & Problem Statement

## Slide 4: Current approaches for the fabrication of carbon nanostructures
V. Galstyan, M. Bhandari, V. Sberveglieri, G. Sberveglieri, E. Comini, Metal Oxide Nanostructures in Food Applications: Quality Control and Packaging, Chemosensors. 6 (2018) 16. https://doi.org/10.3390/chemosensors6020016.
D. Kluge, J.C. Singer, B.R. Neugirg, J.W. Neubauer, H.-W. Schmidt, A. Fery, Top–down meets bottom–up: A comparison of the mechanical properties of melt electrospun and self-assembled 1,3,5-benzenetrisamide fibers, Polymer (Guildf). 53 (2012) 5754–5759. https://doi.org/10.1016/j.polymer.2012.10.016.
Self-assembly
Limited Length and Random Orientation
Photolithography
Physical & Optical Limitations
Two-Photon Polymerization (TPP)
Slow (mm per sec) & Expensive
* Near-Field Electrospinning (NFES)
Suspended Nanowires w/Spatial Control

## Slide 5: Applications of Carbon Nanowires (CNWs)
I.F. Akyildiz, J.M. Jornet, Electromagnetic wireless nanosensor networks, Nano Commun. Netw. 1 (2010) 3–19. https://doi.org/10.1016/j.nancom.2010.04.001.
N. Rikhtegar, M. Keshtgary, A Brief Survey on Molecular and Electromagnetic Communications in Nano-Networks, Int. J. Comput. Appl. 79 (2013) 16–28. https://doi.org/10.5120/13721-1510.
The carbon nanostructure changes its electrical properties with:
deformation (mass, pressure, force or displacement)
absorption/attachment of chemicals
biological processes such as antibody/antigen interaction, DNA interaction and cellular communication

## Slide 6: Introduction: Project overview
To design polymer solutions that can be electrospun by NFES, photopolymerized, and then pyrolyzed into conductive carbon nano-wires.
Polymer Solution
Polymeric micro-fibers
Carbon nano-fibers
Near-Field Electrospinning & Photopolymerization
Pyrolysis and Carbonization
Rheometry
SEM
Raman Spec.
4-Wire Kelvin
SEM
Fabrication Process
Product
Characterization Technique

## Slide 7: Polymer Solution Parameters

## Slide 8: SU-8 Carbon Structures
The production of C-MEMS:
Polymer patterning through photolithography
Carbonization through pyrolysis
However, SU-8 as is can not electrospin
SU-8 does not have the right viscosity & solution conductivity
SU-8 is design for photolithography
Microchem, Su-8 2000.5-2015, 2000.5, 2002, 2005, 2007, 2010, 2015. (2006) 1–5. papers3://publication/uuid/859F51B9-0382-4DE8-88A9-267F936939A3.

## Slide 9: Making SU-8 spunable (by Braulio & Ricardo)
To provided the required viscosity
To increase the solution conductivity
… both needed for smooth PEO flow during electrospinning
SU-8 + TBF + PEO
B. Cárdenas, Advanced Manufacturing Techniques for the Fabrication and Surface Modification of Carbon Nanowires, (2017) 160.
D.R. Flores, Role of rheological properties in near field electrospun fibers morphology, (2017) 130.
Notes: Surface t-

## Slide 10: Results with amended SU-8
The modified solution is spunable
Fiber diameter before pyrolysis of 4.966 μm
Fiber diameter after pyrolysis of 204 nm
But, somewhat pyrolyzable
Fiber resistivity from 407 KΩ to 1.727 MΩ
Fiber yield rate of 81 %
wt% PEO 0.25 | SU-8 2002 [mg] | PEO [mg] | TBT [mg]
 | 2246 | 5.65 | 11.32
= 2 ml of solution
Achieved with:
B. Cárdenas, Advanced Manufacturing Techniques for the Fabrication and Surface Modification of Carbon Nanowires, (2017) 160.

## Slide 11: Implications of PEO, as it introduces oxygen to the solution
The fiber yield rate and fiber conductivity are impacted negatively.
In the presence of oxygen, the char yield decreases. This is due to the oxidation on the char.
High variance in the obtained conductivity across samples.
Some samples are destroyed during pyrolysis
Notes: Surface t-

## Slide 12
Osswald, T., Rudolph, N., Osswald, T., & Rudolph, N. (2014). Generalized Newtonian Fluid (GNF) Models. Polymer Rheology, 59–99. https://doi.org/10.3139/9781569905234.003
The Carreau-Yasuda Model
zero shear rate viscosity
infinite shear rate viscosity
power law region

## Slide 13: Rheology of the amended SU-8 solution (0.25 wt%)
The 0.25 wt% sample (orange line) has a zero-shear viscosity (ZSV) of 60 Pa.s spunable at 600 V
Let’s discover new polymer solutions with similar rheology (and no oxygen)

## Slide 14: Rheology of the proposed polymer solutions
25 wt% in THF & DMF
35 wt% in THF
15 wt% in DMF
8 wt% in CHL
15 wt% in NMP
7 wt% in DCM
Solutions with similar rheology of that of the 0.25wt% PEO SU-8 solution with about 60 Pa.s ZSV each.

## Slide 15: NFES Process Parameters

## Slide 16: Data collection of NFES literature (analysis of ~360 fibers in articles from 2003 to 2020)
Use case 1 (ideal case): The author mentions the process parameters and fiber properties within the article in writing.
Figures from Min2013
Fattahi2017

## Slide 17: Data collection of NFES literature (analysis of ~360 fibers in articles from 2003 to 2020)
Use case 2 (typical case): The author provides the data in plots and graphs.
WebPlotDigitalizer (https://github.com/ankitrohatgi/WebPlotDigitizer):
Applied voltage vs. fiber diameter by Madou2011
M.J. Madou, D. Dunn-Rankin, L. Kulinsky, A. Mirsepassi, G.S. Bisht, S. Oh, G. Canton, Controlled Continuous Patterning of Polymeric Nanofibers on Three-Dimensional Substrates Using Low-Voltage Near-Field Electrospinning, Nano Lett. 11 (2011) 1831–1837. https://doi.org/10.1021/nl2006164.

## Slide 18: Data collection of NFES literature (analysis of ~360 fibers in articles from 2003 to 2020)
Use case 3 (difficult case): The author does not mention the fiber diameter in writing but provides a EM characterization.
Python Image Analysis (with a 4.3% error in avg.):
Figure from Camillo2013
Figures from Min2013
https://github.com/katagirimx/OpenCV-image-measuring
Figure from Camillo2013

## Slide 19
Polymer Concentration,
Nozzle Diameter,
Solution Deposition Rate,
Nozzle to Collector Distance &
Applied Voltage
are the main drivers of the final Fiber Diameter

## Slide 20
low polymer concentrations
slow solution deposition rates
small nozzle
diameters
low voltages

## Slide 21: History of NFES literature (first NFES apparatus built in 2003 by J. Kameoka et al.)
J. Kameoka, R. Orth, Y. Yang, D. Czaplewski, R. Mathers, G.W. Coates, H.G. Craighead, A scanning tip electrospinning source for deposition of oriented nanofibres, Nanotechnology. 14 (2003) 1124–1129. https://doi.org/10.1088/0957-4484/14/10/310.
C. Chang, K. Limkrailassiri, L. Lin, Continuous near-field electrospinning for large area deposition of orderly nanofiber patterns, Appl Phys Lett. (2008) 3. https://doi.org/10.1063/1.2975834.
Thinnest fiber achieved by C. Chang et al. with ~50 nm in diameter. (PEO in water)
However, Fiber yield rate was not reported

## Slide 22: Overall Progress & Next Steps

## Slide 23: Current Work Plan
today
rheology
Literature contributions

## Slide 24
~15 wt% in NMP
~25 wt% in THF & DMF
+35 wt% in THF
+15 wt% in DMF
~8 wt% in CHL
No records
No records
Next step: Study/Test the proposed polymer solutions
high carbon polymers and no oxygen

## Slide 25: Conclusions:
<Conclusion A>
<Conclusion B>

## Slide 27: Carbon nanostructures via Lithography
The production of C-MEMS:
Polymer patterning through photolithography electrospinning
Carbonization through pyrolysis
● SU-8 Waste
● Physical & Optical Limitations
● Structure Limitations
photolithography process

## Slide 28: TPP – Two-Photon Polymerization
B. Cardenas-Benitez, C. Eschenbaum, D. Mager, J.G. Korvink, M.J. Madou, U. Lemmer, I. De Leon, S.O. Martinez-Chapa, Pyrolysis-induced shrinking of three-dimensional structures fabricated by two-photon polymerization: experiment and theoretical model, Microsystems Nanoeng. 5 (2019). https://doi.org/10.1038/s41378-019-0079-9.

## Slide 29: Characterization of the 0.25 wt% PEO Solution
Notes: Surface t-

## Slide 31
25 wt% in THF & DMF
35 wt% in THF
15 wt% in DMF
8 wt% in CHL
15 wt% in NMP
7 wt% in DCM

## Slide 33: Characterization of the 0.25 wt% PEO Solution
Electrospun-able with an applied voltage of 600V.
600V
700V
Unable to initiate the jet at 500V or lower.
Notes: Surface t-

## Slide 36: PEO Solution
The EMS polymer solution consisted of
2ml of SU-8 2002 mixed with
0.5 wt% of Poly(ethylene oxide) (PEO, 4,000,000 MW; SigmaAldrich Inc., Cat. N. 189464) and
0.5 wt% Tetrabutylammonium Tetrafluoroborate salts (TBATFB; SigmaAldrich Inc., Cat. N. 217964) to increase its conductivity and allow smooth polymer flow during electrospinning.
All reagents were used as received. Magnetic stirring of these components was performed for 1hr at 75°C and low rpm (100-150 rpm).

## Slide 37: SU-8 (MicroChem, US)
Notes: https://rsc.aux.eng.ufl.edu/_files/msds/309.pdf

## Slide 38: SU-8 (MicroChem, US)
https://www.fishersci.com/shop/products/NC0702370/nc0702370#?keyword=MICROCHEM+CORP+PHOTORESIST+SU-8
https://www.fishersci.com/shop/products/NC9901158/nc9901158#?keyword=SU-8++developer
Notes: https://rsc.aux.eng.ufl.edu/_files/msds/309.pdf

## Slide 40: References
<reference A>
<reference B>

## Slide 41: <Sub-title>
<content> <key concept>
<content> <key concept>