## Slide 1: Fabrication of graphitic-carbon suspended nanowires through mechano-electrospinning of photo-crosslinkable polymers
Osamu Katagiri-Tanaka A01212611@itesm.mx
Principal Advisor: Dr. Héctor Alán Aguirre Soto Co-advisor and Director of Program: Dra. Dora Iliana Medina Medina
01 Sep 2020

## Slide 2: Agenda
<a point for discussion> : <5min
<another point for discussion> : ~20min

## Slide 3: Introduction: Carbon & Carbon Based Nanomaterials (CBNs)
R.L. McCreery, Advanced Carbon Electrode Materials for Molecular Electrochemistry, Chem. Rev. 108 (2008) 2646–2687. https://doi.org/10.1021/cr068076m.
S. Beigi-boroujeni, O. Katagiri-tanaka, B. Cardenas-benitez, O. Sergio, A. Aguirre-soto, Pyrolytic Carbon from Novolac Epoxy Resin Compressed before Photocrosslinking and Pyrolysis, Mater. Today Proc. (2020).
The crystallite size, molecular arrangement, and anisotropy determine the material’s properties.
The interminable collection of CBNs range from soft, conductive lubricants to very hard, low conductivity solids; and from black colour, bulks to transparent, disordered thin films

## Slide 4: Introduction: Glass-like Carbon
R.L. McCreery, Advanced Carbon Electrode Materials for Molecular Electrochemistry, Chem. Rev. 108 (2008) 2646–2687. https://doi.org/10.1021/cr068076m.
G. Speranza, The Role of Functionalization in the Applications of Carbon Materials: An Overview, C — J. Carbon Res. 5 (2019) 84. https://doi.org/10.3390/c5040084.
Attractive for its electrochemical stability, thermal resistance, electrical conductivity, biocompatibility and is gas impermeable.
It is used in the manufacture of semiconductors.

## Slide 5: Glass-like Carbon NWs: Applications
R.L. McCreery, Advanced Carbon Electrode Materials for Molecular Electrochemistry, Chem. Rev. 108 (2008) 2646–2687. https://doi.org/10.1021/cr068076m.
G. Speranza, The Role of Functionalization in the Applications of Carbon Materials: An Overview, C — J. Carbon Res. 5 (2019) 84. https://doi.org/10.3390/c5040084.

## Slide 6: Introduction: MicroChem’s SU-8 & Tokai’s recipe
<content> <key concept>
R.L. McCreery, Advanced Carbon Electrode Materials for Molecular Electrochemistry, Chem. Rev. 108 (2008) 2646–2687. https://doi.org/10.1021/cr068076m.
G. Speranza, The Role of Functionalization in the Applications of Carbon Materials: An Overview, C — J. Carbon Res. 5 (2019) 84. https://doi.org/10.3390/c5040084.
SU-8
glass-like carbon resistivity:

## Slide 7: Introduction: MicroChem’s SU-8 & Tokai’s recipe
<content> <key concept>
R.L. McCreery, Advanced Carbon Electrode Materials for Molecular Electrochemistry, Chem. Rev. 108 (2008) 2646–2687. https://doi.org/10.1021/cr068076m.
G. Speranza, The Role of Functionalization in the Applications of Carbon Materials: An Overview, C — J. Carbon Res. 5 (2019) 84. https://doi.org/10.3390/c5040084.
SU-8
glass-like carbon resistivity:
Electrical resistivity – comparison:
highly oriented pyrolytic graphite (HOPG)
SU-8 glass-like carbon
TOKAI Glassy carbon
<
10^3
<
x4

## Slide 8: Introduction: Pyrolysis
However, photolithography generates waste in the spin-coating and developing steps. Also, it presents physical & optical limitations to the carbon structures
Microchem, Su-8 2000.5-2015, 2000.5, 2002, 2005, 2007, 2010, 2015. (2006) 1–5. papers3://publication/uuid/859F51B9-0382-4DE8-88A9-267F936939A3.
Pyrolysis of SU8 is currently the typical method to produce glass-like carbon.
Polymer patterning through photolithography
Carbonization through pyrolysis
Limitations can be overcome with other fabrication techniques …

## Slide 9: Current approaches
Self-assembly
Limited Length and Random Orientation
Two-Photon Polymerization (TPP)
Slow (mm per sec) & Expensive
* Near-Field Electrospinning (NFES)
Suspended Nanowires w/Spatial Control
V. Galstyan, M. Bhandari, V. Sberveglieri, G. Sberveglieri, E. Comini, Metal Oxide Nanostructures in Food Applications: Quality Control and Packaging, Chemosensors. 6 (2018) 16. https://doi.org/10.3390/chemosensors6020016.
D. Kluge, J.C. Singer, B.R. Neugirg, J.W. Neubauer, H.-W. Schmidt, A. Fery, Top–down meets bottom–up: A comparison of the mechanical properties of melt electrospun and self-assembled 1,3,5-benzenetrisamide fibers, Polymer (Guildf). 53 (2012) 5754–5759. https://doi.org/10.1016/j.polymer.2012.10.016.

## Slide 10: Best Results so far by NFES by Braulio & Ricardo
Fiber yield rate of 81 %
Fiber diameter before pyrolysis of 4.966 μm
Fiber diameter after pyrolysis of 204 nm
Fiber length of 60.5 ± 4.3 μm
Fiber resistance from 407 KΩ to 1.727 MΩ
wt% PEO 0.25 | SU-8 2002 [mg] | PEO [mg] | TBT [mg]
 | 2246 | 5.65 | 11.32
D.R. Flores, Role of rheological properties in near field electrospun fibers morphology, (2017) 130.
B. Cárdenas Benítez, Advanced Manufacturing Techniques for the Fabrication and Surface Modification of Carbon Nanowires, Tecnológico de Monterrey, 2017.

## Slide 11
low polymer concentrations
slow solution deposition rates
small nozzle
diameters
low voltages
11
NFES Literature Review : Process Parameters

## Slide 12
Polymer Concentration,
Nozzle Diameter,
Solution Deposition Rate,
Nozzle to Collector Distance &
Applied Voltage
are the main drivers of the final Fiber Diameter

## Slide 13: NFES Literature Review : Selection of Polymer-Solvent combinations:
~15 wt% in NMP ()
~25 wt% in THF & DMF (Fong1999)
30 wt% in THF (Yousefi2019)
+15 wt% in DMF
~8 wt% in CHL
No records
No records
Polymers with high carbon content relative to oxygen content
A.A. Yousefi, A.R. Mohebbi, S. Falahdoost Moghadam, S.A. Poursamar, L. Hao, Uniaxially aligned microwire networks for flexible transparent electrodes using a novel electrospinning set-up, Sol. Energy. 188 (2019) 1111–1117. ttps://doi.org/10.1016/j.solener.2019.07.007.
H. Fong, D.H. Reneker, Elastomeric nanofibers of styrene-butadiene-styrene triblock copolymer, J. Polym. Sci. Part B Polym. Phys. 37 (1999) 3488–3493. https://doi.org/10.1002/(SICI)1099-0488(19991215)37:24<3488::AID-POLB9>3.0.CO;2-M.

## Slide 14: Implications of PEO, due to the introduction of oxygen
The fiber yield rate and fiber conductivity are impacted negatively.
In the presence of oxygen, the char yield decreases. This is due to the oxidation on the char.
High variance in the obtained conductivity across samples.
Some samples are destroyed
during pyrolysis

## Slide 15: Conclusions:
<Conclusion A>
<Conclusion B>

## Slide 17: Side slide: Carbon allotropes
R.L. McCreery, Advanced Carbon Electrode Materials for Molecular Electrochemistry, Chem. Rev. 108 (2008) 2646–2687. https://doi.org/10.1021/cr068076m.
S. Beigi-boroujeni, O. Katagiri-tanaka, B. Cardenas-benitez, O. Sergio, A. Aguirre-soto, Pyrolytic Carbon from Novolac Epoxy Resin Compressed before Photocrosslinking and Pyrolysis, Mater. Today Proc. (2020).

## Slide 18: SU-8 (MicroChem, US)
Notes: https://rsc.aux.eng.ufl.edu/_files/msds/309.pdf

## Slide 19: Conclusions:
<content> <key concept> <key concept>

## Slide 20: References
<reference A>
<reference B>