## Slide 1: Fabrication of graphitic-carbon suspended nanowires through mechanoelectrospinning of photocrosslinkable polymers
A Osamu Katagiri Tanaka A01212611@itesm.mx
02 Oct 2019

## Slide 2: Thesis Overview
Design polymer solutions that can be electrospun by NFES, photopolymerized, and then pyrolyzed into carbon nano-wires.

## Slide 3: Previous work
The production of C-MEMS:
Polymer patterning through photolithography electrospinning
Carbonization through pyrolysis
● SU-8 Waste
● Physical & Optical Limitations
● Structure Limitations
photolithography process

## Slide 4: Polymer Solution used by Braulio & Ricardo
wt% PEO 0.25 | SU-8 2002 [mg] | PEO [mg] | TBT [mg]
 | 2246 | 5.65 | 11.32
= 2 ml of solution
Provided the required viscoelasticity
Increase the solution conductivity
… both needed for smooth PEO flow during electrospinning
Notes: Surface t-

## Slide 5: Best Results so far by Braulio & Ricardo
Fiber yield rate of 81 %
Fiber diameter before pyrolisis of 4.966 μm
Fiber diameter after pyrolisis of 204 nm
Fiber length of 60.5 ± 4.3 μm
Fiber resistance from 407 KΩ to 1.727 MΩ

## Slide 6: Implications of PEO, as it introduces oxygen to the solution
The fiber yield rate and fiber conductivity are impacted negatively.
In the presence of oxygen, the char yield decreases. This is due to the oxidation on the char.
High variance in the obtained conductivity across samples.
Some samples are destroyed during pyrolysis
Notes: Surface t-

## Slide 7
14 wt% in THF & DMF (Reneker, 1999)
35 wt% in THF (Megelski, 2002)
No records
3.96 wt% in Styrene (Min, 2013)
12.5 wt% in NMP (Raeesi, 2009)
No records
● FFES
● NFES
Next step: Discover a new polymer solution to beat Braulio’s record
Study solutions with high carbon polymers and no oxygen.

## Slide 8: Characterization of the 0.25 wt% PEO Solution
With zero shear viscosity of 0.88 Pa.s.
Notes: Surface t-

## Slide 9: Q&A

## Slide 10: Characterization of the 0.25 wt% PEO Solution
Electrospun-able with an applied voltage of 600V.
600V
700V
Unable to initiate the jet at 500V or lower.
Notes: Surface t-

## Slide 13: PEO Solution
The EMS polymer solution consisted of
2ml of SU-8 2002 mixed with
0.5 wt% of Poly(ethylene oxide) (PEO, 4,000,000 MW; SigmaAldrich Inc., Cat. N. 189464) and
0.5 wt% Tetrabutylammonium Tetrafluoroborate salts (TBATFB; SigmaAldrich Inc., Cat. N. 217964) to increase its conductivity and allow smooth polymer flow during electrospinning.
All reagents were used as received. Magnetic stirring of these components was performed for 1hr at 75°C and low rpm (100-150 rpm).

## Slide 14
https://www.fishersci.com/shop/products/NC0702370/nc0702370#?keyword=MICROCHEM+CORP+PHOTORESIST+SU-8
https://www.fishersci.com/shop/products/NC9901158/nc9901158#?keyword=SU-8++developer

## Slide 15: Zero shear viscosity measurements and Flores’ measurements
Both measurements have the same behaviour with similar proportions.
However, the results show that the current measured values are approximately three times larger than Flores’ measurements.

## Slide 16: References
Cárdenas, B. (2017). Advanced Manufacturing Techniques for the Fabrication and Surface Modification of Carbon Nanowires, 160.
Flores, D. R. (2017). Role of rheological properties in near field electrospun fibers morphology, 130.

## Slide 17: <subTitle>
<content> <key concept>