## Slide 1: Fabrication of graphitic-carbon suspended nanowires through mechano-electrospinning of photo-crosslinkable polymers
Osamu Katagiri-Tanaka A01212611@itesm.mx
Principal Advisor: Dr. Héctor Alán Aguirre Soto Co-advisor and Director of Program: Dra. Dora Iliana Medina Medina
02 Dec 2020

## Slide 2: Agenda
Motivation & Problem Statement : 10 min
Objectives : 3 min
NFES literature review : 10 min
Rheology Analyses : 10 min
Fabrication & Characterization : 5 min
Conclusions & Future Work : 3 min

## Slide 3: Motivation & Problem Statement

## Slide 4: Glass-like Carbon NWs: Applications
V. Baudrit J, Nanosensors, Int. J. Biosens. Bioelectron. 3 (2017) 368–375.https://doi.org/10.15406/ijbsbe.2017.03.00084.
R.L. McCreery, Chem. Rev. 108 (2008) 2646–2687. https://doi.org/10.1021/cr068076m.
G. Speranza, C — J. Carbon Res. 5 (2019) 84. https://doi.org/10.3390/c5040084.
Notes: Remove general words (Applocations -> detection/sensors)
Problemas que solucionan estos sensores (contaminantes en agua, aire, temperatura en electrónicos, health care)

## Slide 5: Carbon Based Nanomaterials (CBNs)
R.L. McCreery, Chem. Rev. 108 (2008) 2646–2687. https://doi.org/10.1021/cr068076m.
S. Beigi-Boroujeni, O. Katagiri-Tanaka, B. Cardenas-Benitez, S.O. Martinez-Chapa, A. Aguirre-Soto, Mater. Today Proc. (2020). https://doi.org/10.1016/j.matpr.2020.10.014.
The crystallite size, molecular arrangement, and anisotropy determine the material’s properties.
The interminable collection of CBNs range from soft, conductive lubricants to very hard, low conductivity solids; and from black colour, bulks to transparent, disordered thin films
Notes: * Classification in a diagram with ranges and units (characterization techniques)

## Slide 6: Carbon allotropes
R.B. Heimann, S.E. Evsvukov, Y. Koga, Carbon N. Y. 35 (1997) 1654–1658. https://doi.org/10.1016/S0008-6223(97)82794-7.
Е.А. Belenkov, Chelyabinsk State University, Chelyabinsk, Russia, 2003: p. 5.
M. Fedel, Elsevier, 2013: pp. 71–102. https://doi.org/10.1533/9780857093516.1.71.
M. Razeghi, Springer International Publishing, Cham, 2019. https://doi.org/10.1007/978-3-319-75708-7.
K. Alstrup Jensen, J. Bøgelund, P. Jackson, N. Raun Jacobsen, R. Birkedal, P. Axel Clausen, A. Thoustrup Saber, H. Wallin, U. Birgitte Vogel, The Danish Environmental Protection Agency, 2015.

## Slide 7: Carbon allotropes
R.L. McCreery, Chem. Rev. 108 (2008) 2646–2687. https://doi.org/10.1021/cr068076m.
S. Beigi-Boroujeni, O. Katagiri-Tanaka, B. Cardenas-Benitez, S.O. Martinez-Chapa, A. Aguirre-Soto, Mater. Today Proc. (2020). https://doi.org/10.1016/j.matpr.2020.10.014.
Harry Marsh. Elsevier, Apr. 1989, p. 43. ISBN: 9780408038379. DOI: 10.1016/C2013- 0- 04111- 4. URL: https: //linkinghub.elsevier.com/retrieve/pii/C20130041114.
Pierson Hugh. Elsevier, 1994, p. 419. ISBN: 9780815513391.
Notes: Add Triangle diagram
Focus in GLC

## Slide 8: Glass-like Carbon
R.L. McCreery, Chem. Rev. 108 (2008) 2646–2687. https://doi.org/10.1021/cr068076m.
G. Speranza, C — J. Carbon Res. 5 (2019) 84. https://doi.org/10.3390/c5040084.
Attractive for its electrochemical stability, thermal resistance, electrical conductivity, biocompatibility and is gas impermeable.
It is used in the manufacture of semiconductors.

## Slide 9: MicroChem’s SU-8 & Tokai’s recipe
R.L. McCreery, Chem. Rev. 108 (2008) 2646–2687. https://doi.org/10.1021/cr068076m.
S. Beigi-Boroujeni, O. Katagiri-Tanaka, B. Cardenas-Benitez, S.O. Martinez-Chapa, A. Aguirre-Soto, Mater. Today Proc. (2020). https://doi.org/10.1016/j.matpr.2020.10.014.
G. Speranza, C — J. Carbon Res. 5 (2019) 84. https://doi.org/10.3390/c5040084.
Electrical resistivity, comparison:
highly oriented pyrolytic graphite (HOPG)
SU-8 glass-like carbon
TOKAI Glassy carbon
<
x103
<
x4
Tokai’s recipe is a secret …
Notes: * Focus in microchem

## Slide 10: MicroChem’s SU-8 & Tokai’s recipe
<content> <key concept>
R.L. McCreery, Advanced Carbon Electrode Materials for Molecular Electrochemistry, Chem. Rev. 108 (2008) 2646–2687. https://doi.org/10.1021/cr068076m.
S. Beigi-Boroujeni, O. Katagiri-Tanaka, B. Cardenas-Benitez, S.O. Martinez-Chapa, A. Aguirre-Soto, Mater. Today Proc. (2020). https://doi.org/10.1016/j.matpr.2020.10.014.
G. Speranza, The Role of Functionalization in the Applications of Carbon Materials: An Overview, C — J. Carbon Res. 5 (2019) 84. https://doi.org/10.3390/c5040084.
SU-8
glass-like carbon resistivity:

## Slide 11: Current approaches
V. Galstyan, M. Bhandari, V. Sberveglieri, G. Sberveglieri, E. Comini, Metal Oxide Nanostructures in Food Applications: Quality Control and Packaging, Chemosensors. 6 (2018) 16. https://doi.org/10.3390/chemosensors6020016.
D. Kluge, J.C. Singer, B.R. Neugirg, J.W. Neubauer, H.-W. Schmidt, A. Fery, Top–down meets bottom–up: A comparison of the mechanical properties of melt electrospun and self-assembled 1,3,5-benzenetrisamide fibers, Polymer (Guildf). 53 (2012) 5754–5759. https://doi.org/10.1016/j.polymer.2012.10.016.
Photolithography
Physical & Optical Limitations
Two-Photon Polymerization (TPP)
Slow (mm per sec) & Expensive
*Near-Field Electrospinning (NFES)
Suspended Nanowires w/Spatial Control

## Slide 12: MicroChem’s SU-8
However, photolithography generates waste in the spin-coating and developing steps. Also, it presents structural limitations.
Microchem, Su-8 2000.5-2015, 2000.5, 2002, 2005, 2007, 2010, 2015. (2006) 1–5. papers3://publication/uuid/859F51B9-0382-4DE8-88A9-267F936939A3.
Pyrolysis of SU8 is currently the typical method to produce glass-like carbon.
Polymer patterning through photolithography
Carbonization through pyrolysis
Limitations can be overcome with other fabrication techniques, such as NFES

## Slide 13: MicroChem’s SU-8
& PEO to provided the required viscosity
SU-8 + TBF + PEO formulation:
TBF to increase the solution conductivity
… both needed for smooth PEO flow during electrospinning
However, SU-8 as is not electrospinnable
SU-8 does not have the right viscosity & solution conductivity.
SU-8 is design for photolithography.
D.R. Flores, Role of rheological properties in near field electrospun fibers morphology, (2017) 130.
B. Cárdenas Benítez, Advanced Manufacturing Techniques for the Fabrication and Surface Modification of Carbon Nanowires, Tecnológico de Monterrey, 2017.
Notes: Remove background from figures
Para las aplicationes necesito que sea electrospinnalbe
Photolithography-able vs. Electrospinnableility
Highlight the PEO

## Slide 14: Problem Statement
The interdependence between the process and solution parameters presents a challenge to predict the fiber diameter.
Properties of an electrospun fiber depend on many parameters,
and each parameter also depends on the polymer-solvent system.
S.B. Gadkari, Scaling analysis for electrospinning, Springerplus. 3 (2014) 705. https://doi.org/10.1186/2193-1801-3-705.
Solution Parameters:
Concentration
Molecular weight
Viscosity
Electrical conductivity
Ambient Parameters:
Humidity
Temperature
Process Parameters:
Applied Voltage
Flow rate
Working distance
Notes: Predicción de diámetro y control espacial
Mention my important parameters: conductivity low diameter spatial control
Challenge de control de diametro

## Slide 15: Best Results so far by NFES (previous work)
Fiber yield rate of 81 %
Fiber diameter before pyrolysis of 4.966 μm
Fiber diameter after pyrolysis of 204 nm
Fiber length of 60.5 ± 4.3 μm
Fiber resistance from 407 KΩ to 1.727 MΩ
wt% PEO 0.25 | SU-8 2002 [mg] | PEO [mg] | TBF [mg]
 | 2246 | 5.65 | 11.32
D.R. Flores, Role of rheological properties in near field electrospun fibers morphology, (2017) 130.
B. Cárdenas Benítez, Advanced Manufacturing Techniques for the Fabrication and Surface Modification of Carbon Nanowires, Tecnológico de Monterrey, 2017.

## Slide 16: Implications of PEO
The fiber yield rate and fiber conductivity are impacted negatively as PEO introduces more oxygen to the solution
The addition of oxygen modifies the carbon structure.
High variance in the obtained conductivity across samples.
Some samples are destroyed during pyrolysis
D.R. Flores, Role of rheological properties in near field electrospun fibers morphology, (2017) 130.
B. Cárdenas Benítez, Advanced Manufacturing Techniques for the Fabrication and Surface Modification of Carbon Nanowires, Tecnológico de Monterrey, 2017.
Notes: Diagram – PEO pyrolysis
Mention the rol of Oxygen – abd connect it witht the desired characteristics – closed porous
Pyrolysis stages
Balance of properties

## Slide 17: Objectives

## Slide 18: Objectives
General. Formulate polymer/solvent combinations that have the greatest potential to replace or modify the SU-8/PEO formulation for the fabrication of microscopic polymer fibers that may be converted to conductive suspended carbon nano-wires.
Specific1. Learn how the diameter of the electrospun polymer fiber can be controlled by appropriate tuning of the NFES parameters and solution properties.
Specific2. Through rheological analyses, determine if polymer solutions have comparative viscoelastic properties to those of the SU-8/PEO benchmark, and if they can be easily electrospun by NFES.
Specific3. Propose alternatives to the SU-8/PEO benchmark formulation for the production of microscopic polymer fibers with potential for the fabrication of carbon nano-wires.

## Slide 19: NFES literature review
Specific Objective 1. Learn how the diameter of the electrospun polymer fiber can be controlled by appropriate tuning of the NFES parameters and solution properties.
Notes: To find substitutions to keep
Spatial control, high conductivity, low diameter
Find new formulations or replace PEO in SU8 -> find new materials

## Slide 20: Methods: NFES literature (first NFES apparatus built in 2003 by J. Kameoka et al.)
J. Kameoka, R. Orth, Y. Yang, D. Czaplewski, R. Mathers, G.W. Coates, H.G. Craighead, Nanotechnology. 14 (2003) 1124–1129. https://doi.org/10.1088/0957-4484/14/10/310.
C. Chang, K. Limkrailassiri, L. Lin, Appl Phys Lett. (2008) 3. https://doi.org/10.1063/1.2975834.
Thinnest fiber achieved by C. Chang et al. with ~50 nm in diameter. (PEO in water)
However, fiber yield rate was not reported

## Slide 21: Methods: Data collection (analysis of NFES articles from 2003 to 2020)
The author mentions the process parameters and fiber properties within the article in writing.
Figures from Min2013
Fattahi2017
S.-Y. Min, T.-S. Kim, B.J. Kim, H. Cho, Y.-Y. Noh, H. Yang, J.H. Cho, T.-W. Lee,, Nat. Commun. 4 (2013) 1773. https://doi.org/10.1038/ncomms2785.
P. Fattahi, J.T. Dover, J.L. Brown, Adv. Healthc. Mater. 6 (2017) 1700456. https://doi.org/10.1002/adhm.201700456.

## Slide 22: Methods: Data collection (analysis of NFES articles from 2003 to 2020)
The author provides the data in plots and graphs.
WebPlotDigitalizer (https://github.com/ankitrohatgi/WebPlotDigitizer):
Applied voltage vs. fiber diameter by Madou2011
M.J. Madou, D. Dunn-Rankin, L. Kulinsky, A. Mirsepassi, G.S. Bisht, S. Oh, G. Canton, Nano Lett. 11 (2011) 1831–1837. https://doi.org/10.1021/nl2006164.

## Slide 23: Methods: Data collection (analysis of NFES articles from 2003 to 2020)
360.29 nm
The author does not mention the fiber diameter in writing but provides a EM characterization.
Python Image Analysis (with a 3.2% error in avg.):
Figures from Camillo2013
Figures from Min2013
S.-Y. Min, T.-S. Kim, B.J. Kim, H. Cho, Y.-Y. Noh, H. Yang, J.H. Cho, T.-W. Lee, Nat. Commun. 4 (2013) 1773. https://doi.org/10.1038/ncomms2785..
https://github.com/katagirimx/OpenCV-image-measuring
D. Di Camillo, V. Fasano, F. Ruggieri, S. Santucci, L. Lozzi, A. Camposeo, D. Pisignano, Nanoscale. 5 (2013) 11637–11642. https://doi.org/10.1039/C3NR03094F.
493.2 nm
63.21 nm
127.10 nm

## Slide 24: Methods: Data collection (analysis of NFES articles from 2003 to 2020)
Image analysis algorithm:
Segmentation is done manually with a image processing software
Pre-processing takes the binary image
Object detection is done with the Sobel/Canny algorithm
Measurement is to compute the pixel-to- metric proportions, using the scalebar as reference

## Slide 25: Relevant Parameters:
Zero-shear viscosity,
Polymer Concentration,
Solution Flow Rate,
&
Applied Voltage
are the main drivers of the final Fiber Diameter
Matrix of Pearson linear correlation coefficients, built with Python’s seaborn package.

## Slide 26: Conclusion 1.2: Let’s focus on polymer concentration
Polymer concentration is the most reliable process parameter to control the morphology of electrospun fibers. (regardless the type of NFES process)
Notes: Song2015 : glass capillary tip
Brown201X : melt ES
Husain2016 : L = cm
Shin2019 : coiled/meander fibers
Parajuli2016 : concentrations 25 – 80%

## Slide 27: Conclusion 1.2: Let’s focus on polymer concentration
Polymer concentration is the most reliable process parameter to control the morphology of electrospun fibers. (regardless the type of NFES process)
Notes: Song2015 : glass capillary tip
Brown201X : melt ES
Husain2016 : L = cm
Shin2019 : coiled/meander fibers
Parajuli2016 : concentrations 25 – 80%

## Slide 28
low polymer
concentrations
slow solution flow rates
small needle
diameters
low voltages
28
Conclusion 1.1:
Process Parameters

## Slide 29: Diameter Prediction of Electrospun Fibers
Siddharth B. Gadkari. In: SpringerPlus 3.1 (Dec. 2014), p. 705. ISSN: 2193-1801. DOI: 10.1186/2193-1801-3-705.
B. Zhang, F. Kang, J.-M. Tarascon, J.-K. Kim, Prog. Mater. (2016) https://doi.org/10.1016/j.pmatsci.2015.08.002.
M.E. Helgeson, K.N. Grammatikos, J.M. Deitzel, N.J. Wagner, Polymer (2008) https://doi.org/10.1016/j.polymer.2008.04.025.
T.D. Brown, F. Edin, N. Detta, A.D. Skelton, D.W. Hutmacher, P.D. Dalton, Mater. Sci. Eng. C. 45 (2014) 698–708. https://doi.org/10.1016/j.msec.2014.07.034.
The fiber morphology not only depends on the process parameters, but also on the type of electrospinning process and on polymer-solvent system.
The existing interdependence between the process and solution parameters adds complexity and ambiguity to the effect of each parameter
“[…] while decreasing the voltage could also be used to reduce the average fiber diameter.”
Brown et al.
“[…] the fiber diameter decreases as the applied voltage increases.”
Helgeson et al.
“[…] neither the collecting distance nor the applied voltage has large influences on fiber diameter […]”
Zhang et al.

## Slide 30: Diameter Prediction of Electrospun Fibers
M.E. Helgeson, N.J. Wagner, AIChE J. 53 (2007) 51–55. https://doi.org/10.1002/aic.11056.
Helgeson and Wagner have presented an adimensional analysis to
predict the fiber diameter with conservation equations of momentum, mass, electric charge and four dimensionless numbers:
Helgeson get rid of unknown and/or hard to measure parameters, such as the initial jet velocity.
Correlation between the electrostatic and viscous forces:
Ohnesorge number (jet behaviour and capillary rupture):

## Slide 31: Diameter Prediction of Electrospun Fibers
M.E. Helgeson, N.J. Wagner, AIChE J. 53 (2007) 51–55. https://doi.org/10.1002/aic.11056.

## Slide 32: Diameter Prediction of Electrospun Fibers
M.E. Helgeson, N.J. Wagner, AIChE J. 53 (2007) 51–55. https://doi.org/10.1002/aic.11056.
Notes: both types of electrospinning behave in a similar manner
the FFES data fits better a linear behavior of slope -1.
As the working distance closes in NFES, the data points fit a shallower slope with higher P1 values and lower Oh values
that in NFES less viscous solutions have been used

## Slide 33: Rheology Analyses
Specific Objective 2. Through rheological analyses, determine if polymer solutions have comparative viscoelastic properties to those of the SU-8/PEO benchmark, and if they can be easily electrospun by NFES.

## Slide 34: Selection of Polymer-Solvent combinations
N. Liu, K. Kim, H.Y. Jeong, P.C. Hsu, Y. Cui, Z. Bao,, ACS Nano. 9 (2015) 9043–9049. https://doi.org/10.1021/acsnano.5b03134.
higher sp2 carbon content translates into higher graphitization degree and higher electrical conductivity
polymers with functional groups are required for the creation of smooth and continuous fibers.
Zhenan Bao et al. investigated the effect of the polymer chemical
Structure of:
Notes: Bao lit review
Mention templating effect & pipeline stacking
PVP and Novolac have one benzene ring in each repeating unit,
PVA is mainly made out of sp3 carbon
PS is not functionalized

## Slide 35: Conclusion1.3: Selection of Polymer-Solvent combinations
Polymers with high carbon content relative to oxygen content
A.A. Yousefi, A.R. Mohebbi, S. Falahdoost Moghadam, S.A. Poursamar, L. Hao, Sol. Energy. 188 (2019) 1111–1117. ttps://doi.org/10.1016/j.solener.2019.07.007.
H. Fong, D.H. Reneker, J. Polym. Sci. Part B Polym. Phys. 37 (1999) 3488–3493. https://doi.org/10.1002/(SICI)1099-0488(19991215)37:24<3488::AID-POLB9>3.0.CO;2-M.
S.-Y. Min, T.-S. Kim, B.J. Kim, H. Cho, Y.-Y. Noh, H. Yang, J.H. Cho, T.-W, Nat. Commun. 4 (2013) 1773. https://doi.org/10.1038/ncomms2785.
Notes: Mw
Aromaticidad
Cantidad de carbono
Ratio oxygen / carbon in pyrolysis

## Slide 36
Under some critical concentration NFES yields beads or small fibres
Over some critical concentration NFES continuous fibres
Viscosity increases with molecular weight
The general belief is that the molecular weight needs to be sufficient enough to create or induce entanglements
D.R. Flores, Role of rheological properties in near field electrospun fibers morphology, (2017) 130.
G.L. Wilkes, J. Chem. Educ. 58 (1981) 880. https://doi.org/10.1021/ed058p880.
Literature claims

## Slide 37
As “electrospinnability” is determined by the polymer chain entanglement,
chain entanglement is controlled by molecular weight,
increasing molecular weight increases viscosity, and
viscosity is controlled by polymer concentration, then
The critical/spinnable concentration can be found in a viscosity vs. concentration plot
critical
concentration
Literature claims
D.R. Flores, Role of rheological properties in near field electrospun fibers morphology, (2017) 130.
G.L. Wilkes, J. Chem. Educ. 58 (1981) 880. https://doi.org/10.1021/ed058p880.

## Slide 38: Methods: Sample Preparation (SU8-PEO)
3.0 ml samples
A salt (TBF) was added to all the samples to increase the electrical conductivity
on a heating plate at 160 rpm and 60°C, for 2 hours each.

## Slide 39: Methods: Sample Preparation (PS & PSB)

## Slide 40: Methods: Sample Preparation (PSB & PSMS)

## Slide 41: Methods: Sample Preparation (PVK & SU8-PVK)

## Slide 42: Methods: Rheology – Frequency Sweeps
Geometry:
Steel cone plate, Peltier plate
(60.0 mm diameter, 0.9979° cone angle, 23 µm truncation)
Procedure:
Frequency sweep
(20°C, for 20 min
from to 1/s shear rates)

## Slide 43: Methods: Rheology – Instrumentation
Measured Parameter | Calculated Parameter
Torque Angular displacement Angular velocity | Stress Strain Shear rate
Discovery Hybrid Rheometers – TA Instruments, (n.d.). https://www.tainstruments.com/products/rheology/discovery-hybrid-rheometers/ (accessed 18 May 2020).
Malvern Instruments Worldwide, Malvern Instruments White Paper, (2016) 1–20. https://www.malvernpanalytical.com/en/learn/knowledge-center/whitepapers/WP160620BasicIntroRheology.html.

## Slide 44: Methods: Rheology – Geometry Selection
Discovery Hybrid Rheometers – TA Instruments, (n.d.). https://www.tainstruments.com/products/rheology/discovery-hybrid-rheometers/ (accessed 18 May 2020).
Geometry options:
Concentric Cylinders
Cone and Plate
Parallel Plate
Torsion Rectangular
Very Low Viscosity
Solids

## Slide 45: Methods: Rheology – Radial Migration Effect
R. W. Connelly and J. Greener. In: Journal of Rheology 29.2 (1985), pp. 209–226. ISSN: 0148-6055. DOI: 10.1122/1.549828.
Christopher J Pipe, Trushant S Majmudar, and Gareth H. McKinley. In: Rheologica Acta 47.5-6 (July 2008), pp. 621–642. ISSN: 0035-4511. DOI: 10.1007/s00397- 008- 0268-1
High centrifugal stresses result in the sample being thrown out of the measuring area; a phenomenon known as ’radial migration effect’.
Once the ’radial migration effect’ partially ejects the sample, the viscosity measurements are lower than expected due to a drop in torque.

## Slide 46
Methods: The Carreau-Yasuda Model
: viscosity
: shear rate
: infinite shear rate viscosity
: zero shear rate viscosity
: time constant
: Power Law index
: width of the transition region

## Slide 47
Methods: Other models:

## Slide 48
Methods: Other models:

## Slide 49
Methods: Rheology results validation for 0wt% PEO
MicroChem data sheet:
Measured:
Microchem, Su-8 2000.5, 2002, 2005, 2007, 2010, 2015, Microchem. (2018) 1–5. papers3://publication/uuid/859F51B9-0382-4DE8-88A9-267F936939A3.
vs.
from PEO in SU8
sample set
from PVK in SU8
sample set
and 0wt% PVK

## Slide 50
Methods: Rheology results validation for 0wt% PVK
Anton-Paar data sheet:
Measured CHL viscosity:
https://wiki.anton-paar.com/en/chloroform/
vs.

## Slide 51
spinnable
concentrations
non-spinnable concentrations
c*=25 wt%
Spinnable/Critical Concentration

## Slide 52
Spinnable/Critical Concentration

## Slide 53
Conclusion2.1: Spinnable/Critical Concentration
Vu Anh Doan et al. In: Journal of Materials Science 48.5 (Mar. 2013), pp. 2046–2052. ISSN: 0022-2461. DOI: 10.1007/s10853- 012- 6974- 1. URL: http://link.springer.com/10.1007/s10853-012-6974-1.
Ralph H. Colby, Lewis J. Fetters, and William W. Graessley. In: Macromolecules 20.9 (Sept. 1987), pp. 2226–2237. ISSN: 0024-9297. DOI: 10 . 1021 / ma00175a030.
A low molecular weight shall be compensated with higher concentrations to reach a spunable viscosity.

## Slide 54
c*

## Slide 55
c*

## Slide 56
c*

## Slide 57
c*

## Slide 58
c*

## Slide 59
c*

## Slide 60: Fabrication & Characterization
Specific Objective 3. Propose alternatives to the SU-8/PEO benchmark formulation for the production of microscopic polymer fibers with potential for the fabrication of carbon nano-wires.

## Slide 61
Methods: Design of experiments / NFES
Given the results of previous work, the experiments shall reflect:
The SU8-PEO sample set is the control
The calculated critical concentration were used for each sample set.
Each sample was electrospun at different applied voltages from 200 to 600V
  Other process parameters (working distance, stage velocity, flow rate) are to be tuned and remain constant during NFES.
Domingo R Flores-hernandez et al. In: (2020). DOI: 10.3390/polym12061358.

## Slide 62: Fabrication: Process Parameters
Fabrication velocity: 10 mm/s
Working distance: 0.5 mm
Applied voltage: 200V to 600V
Applied current: 10 uA
Flow rate: 0.04 uL/min
Spacing: 10um
0.25 wt% PEO in SU-8
600V
900V

## Slide 63: Characterization:
PEO in SU-8

## Slide 64
PSB in THF and DMF
PS in THF

## Slide 65
PVK in CHL
PVK in SU-8

## Slide 66: non-spinnable solutions
Polymer / Solvent | Critical concentration | Rationale
Poly(Styrene-co-alpha-Methylstyrene) (PSMS) in N,N-Dimethylformamide(DMF) | 5 wt% (and 10, 15 wt%) | Fibres were broken into agglomerates / dust
Poly(Styrene-co-Butadiene) (PSB) in 1-Methyl-2-Pyrrolidinone (NMP) | 8.00 wt% | Development of a shell around the drop.
PSMS
Notes: Poly(Styrene-co-Butadiene)
1-Methyl-2-Pyrrolidinone
7.74 wt%

## Slide 67: Results: Spinnable solutions

## Slide 68: Conclusions & Future Work

## Slide 69
Helgeson’s Dimensionless analysis
Helgeson’s model was thought to work with far-field electrospinning, hence the deviation of the NFES data from the model trend.
For an accurate NFES fiber diameter prediction, the mechanical stresses introduced by the moving stage shall be considered in the model

## Slide 70
Pyrolysis Process
This work verifies the electro-spinnability of four new formulations and one modification to the PEO/SU-8 solution, however fibers were not carbonized into carbon structures.
Further work shall study the pyrolysis process of the proposed fibers to get carbon structures with good electrical conductivity.
A photo-polymerization process could be introduced before pyrolysis to increase the order of the molecules and achieve carbon with higher
conductivity.

## Slide 71
Process Parameters
The viscosity-concentration plot is a helpful tool to estimate the critical spinnable concentration of a polymer-solvent system as NFES solutions require specific viscosities to initiate a polymer jet. However there is room for improvement as this method only considers rheological data.
Other methods could be adopted to better tune other process parameters such as stage velocity, and applied voltage.

## Slide 73: Any Questions?
Osamu Katagiri-Tanaka A01212611@itesm.mx
02 Dec 2020

## Slide 74: SU-8 (MicroChem, US)
Notes: https://rsc.aux.eng.ufl.edu/_files/msds/309.pdf

## Slide 75: Carbon nanostructures via Lithography
The production of C-MEMS:
Polymer patterning through photolithography electrospinning
Carbonization through pyrolysis
● SU-8 Waste
● Physical & Optical Limitations
● Structure Limitations
photolithography process

## Slide 76: TPP – Two-Photon Polymerization
B. Cardenas-Benitez, C. Eschenbaum, D. Mager, J.G. Korvink, M.J. Madou, U. Lemmer, I. De Leon, S.O. Martinez-Chapa, Pyrolysis-induced shrinking of three-dimensional structures fabricated by two-photon polymerization: experiment and theoretical model, Microsystems Nanoeng. 5 (2019). https://doi.org/10.1038/s41378-019-0079-9.

## Slide 77: Characterization of the 0.25 wt% PEO Solution
Notes: Surface t-

## Slide 79
wt% in THF & DMF
wt% in THF
wt% in DMF
wt% in CHL
wt% in NMP
wt% in SU-8

## Slide 81
D.R. Flores, Role of rheological properties in near field electrospun fibers morphology, (2017) 130.
Notes: D.R. Flores, Role of rheological properties in near field electrospun fibers morphology, (2017) 130.

## Slide 82
Methods: Rheology results validation
D.R. Flores-hernandez, B. Cardenas-benitez, S.O. Martinez-chapa, J. Bonilla-rios, Tailoring the Diameters of Electro-Mechanically Spun Fibers by Controlling Their Deborah Numbers, (2020). https://doi.org/10.3390/polym12061358.
Notes: D.R. Flores-hernandez, B. Cardenas-benitez, S.O. Martinez-chapa, J. Bonilla-rios, Tailoring the Diameters of Electro-Mechanically Spun Fibers by Controlling Their Deborah Numbers, (2020). https://doi.org/10.3390/polym12061358.

## Slide 83
Methods: Rheology results validation
G.S. Bisht, G. Canton, A. Mirsepassi, L. Kulinsky, S. Oh, D. Dunn-Rankin, M.J. Madou, D. Dunn-Rankin, L. Kulinsky, A. Mirsepassi, G.S. Bisht, S. Oh, G. Canton, Controlled Continuous Patterning of Polymeric Nanofibers on Three-Dimensional Substrates Using Low-Voltage Near-Field Electrospinning, Nano Lett. 11 (2011) 1831–1837. https://doi.org/10.1021/nl2006164.
Notes: D.R. Flores-hernandez, B. Cardenas-benitez, S.O. Martinez-chapa, J. Bonilla-rios, Tailoring the Diameters of Electro-Mechanically Spun Fibers by Controlling Their Deborah Numbers, (2020). https://doi.org/10.3390/polym12061358.

## Slide 86: SU-8 (MicroChem, US)
https://www.fishersci.com/shop/products/NC0702370/nc0702370#?keyword=MICROCHEM+CORP+PHOTORESIST+SU-8
https://www.fishersci.com/shop/products/NC9901158/nc9901158#?keyword=SU-8++developer
Notes: https://rsc.aux.eng.ufl.edu/_files/msds/309.pdf

## Slide 87: Materials

## Slide 88: title:
<content> <key concept> <key concept>
<a point>
<another point>
D.R. Flores-hernandez, B. Cardenas-benitez, S.O. Martinez-chapa, J. Bonilla-rios, Tailoring the Diameters of Electro-Mechanically Spun Fibers by Controlling Their Deborah Numbers, (2020). https://doi.org/10.3390/polym12061358.