## Slide 1: Research Overview & Related Article
A. Osamu Katagiri Tanaka A01212611itesm.mx
April 04, 2019

## Slide 2: Agenda
My Thesis Overview : ~5min
Related Article : ~20min
Q&A : ~10min

## Slide 3: Thesis Overview
Study the practice and feasibility of a new fabrication process to achieve mass scale manufacturing of carbon nano-wires in an inexpensive, continuous, simple and reproducible manner

## Slide 4: Thesis Overview
Design polymer solutions that can be electrospun by NFES, photopolymerized, and then pyrolyzed into carbon nano-wires.

## Slide 5: Related Article
Pramanick, B., Vazquez-Pinon, M., Torres-Castro, A., & Martinez-Chapaa, S. O. (2018). Effect of pyrolysis process parameters on electrical, physical, chemical and electro-chemical properties of SU-8-derived carbon structures fabricated using the C-MEMS process. Materials Today: Proceedings, 5(3), 9669–9682. https://doi.org/10.1016/J.MATPR.2017.10.153

## Slide 6: Pyrolysis
Is the chemical decomposition of any organic polymer by heating in an oxygen-free environment
This degradation technique can lead to the formation condensable gases and carbonized materials
Basu, P. (2018). Biomass Gasification, Pyrolysis and Torrefaction - Practical Design and Theory (3rd Edition). Elsevier. Retrieved from https://app.knovel.com/hotlink/pdf/id:kt011PGVNJ/biomass-gasification/biomass-ga-historical

## Slide 7: Pyrolysis parameters that were investigated
Maximum Pyrolysis Temperature
Temperature Ramp Rate
Gas () flow rate
Pramanick, B., Vazquez-Pinon, M., Torres-Castro, A., & Martinez-Chapaa, S. O. (2018). Effect of pyrolysis process parameters on electrical, physical, chemical and electro-chemical properties of SU-8-derived carbon structures fabricated using the C-MEMS process. Materials Today: Proceedings, 5(3), 9669–9682. https://doi.org/10.1016/J.MATPR.2017.10.153

## Slide 8: Experiment - Step 1: photolithography
Fabrication of SU-8 polymeric structures

## Slide 9: Experiment - Step 2: pyrolysis
Fabrication of carbon structures

## Slide 10: Experiment - Step 2: pyrolysis
Sample | Maximum Temperature | Temperature Ramp Rate | Gas () flow rate
0 | 600 °C | 5 °C/min | 6 l/min
1 | 700 °C |  | 
2 | 800 °C |  | 
3 | 900 °C |  | 
4 | 900 °C | 2.5 °C/min | 6 l/min
5 |  | 5 °C/min | 
6 |  | 10 °C/min | 
7 |  | 20 °C/min | 
8 | 900 °C | 5 °C/min | 3 l/min
9 |  |  | 4.5 l/min
10 |  |  | 6 l/min
11 |  |  | 7.5 l/min
Sample | Maximum Temperature | Temperature Ramp Rate | 
0 | 600 °C | 5 °C/min | 6 l/min
1 | 700 °C |  | 
2 | 800 °C |  | 
3 | 900 °C |  | 
4 | 900 °C | 2.5 °C/min | 6 l/min
5 |  | 5 °C/min | 
6 |  | 10 °C/min | 
7 |  | 20 °C/min | 
8 | 900 °C | 5 °C/min | 3 l/min
9 |  |  | 4.5 l/min
10 |  |  | 6 l/min
11 |  |  | 7.5 l/min

## Slide 11: Results - Step 3: discussion
Effect of maximum pyrolysis temperature

## Slide 12: Results - Step 3: discussion
Effect of maximum pyrolysis temperature

## Slide 13: Results - Step 3: discussion
Effect of maximum pyrolysis temperature

## Slide 14: Q&A

## Slide 15: Decomposition of large hydrocarbon molecules into smaller ones during pyrolysis
Basu, P. (2018). Biomass Gasification, Pyrolysis and Torrefaction - Practical Design and Theory (3rd Edition). Elsevier. Retrieved from https://app.knovel.com/hotlink/pdf/id:kt011PGVNJ/biomass-gasification/biomass-ga-historical
Pyrolysis Products
Liquids
  Heavier hydrocarbons
  water
Solids
  char & carbon
Gases
  , , , , , ,

## Slide 16: Characteristics of some thermal decomposition processes
Mohan, D., Pittman Jr., C.U., Steele, P.H., 2003. Pyrolysis of Wood/Biomass for Bio- oil: A Critical Review. Energy Fuels 20, 848–889.

## Slide 17: Pyrolysis
Rapid heating -> higher volatiles (more liquids)
Low temperatures -> greater amount of char, gas yield decreases
Basu, P. (2018). Biomass Gasification, Pyrolysis and Torrefaction - Practical Design and Theory (3rd Edition). Elsevier. Retrieved from https://app.knovel.com/hotlink/pdf/id:kt011PGVNJ/biomass-gasification/biomass-ga-historical
Small particles -> higher liquid yield

## Slide 18: Photolithography: Step by step
Jae-Hwang Lee. (2015). Photolithography: Step by step - YouTube. Retrieved from https://www.youtube.com/watch?v=oBKhN4n-EGI

## Slide 19: Experiment : characterization
Pore size distribution
  Optical images of the surface by confocal microscopy
Resistivity measurements
  4-point probe method
Crystallinity variation
  Raman spectroscopy w/a 514 nm Ar laser source
Chemical composition (quantify the elements present on the surface of the structures)
  Energy-dispersive X-ray spectroscopy

## Slide 20: Experiment : parameters to study
Three pyrolysis parameters
  Maximum temperature
    600°C, 700°C, 800°C and 900°C
    Temperature ramp rate constant @ 5°C/min
    Nitrogen flow rate constant @ 6l/m
  Temperature ramp rate
    2.5°C/min, 5°C/min, 10°C/min and 20°C/min
    Maximum temperature constant @ 900°C
    Nitrogen flow rate constant @ 6l/min
  Nitrogen flow rate
    3l/min, 4.5l/min, 6l/min and 7.5l/min
    Maximum temperature constant @ 900°C
    Temperature ramp rate constant @ 5°C/min

## Slide 21: References
Pramanick, B., Vazquez-Pinon, M., Torres-Castro, A., & Martinez-Chapaa, S. O. (2018). Effect of pyrolysis process parameters on electrical, physical, chemical and electro-chemical properties of SU-8-derived carbon structures fabricated using the C-MEMS process. Materials Today: Proceedings, 5(3), 9669–9682. https://doi.org/10.1016/J.MATPR.2017.10.153
Ulyanov, V., Koshelev, M., Kharchuk, S., Gulevskii, V., & Timochkin, A. (2018). Study of the pyrolysis of solid organic polymers by their heating with metal melt. Petroleum Chemistry, 58(1), 68–75. https://doi.org/10.1134/S0965544118010140