## Slide 1: Rheology [experiment]
A. Osamu Katagiri Tanaka A01212611itesm.mx
April 25, 2019

## Slide 2: Agenda
My Thesis Overview : <3min
Experiment : ~10min
Q&A : ~10min

## Slide 3: Thesis Overview
Design polymer solutions that can be electrospun by NFES, photopolymerized, and then pyrolyzed into carbon nano-wires.

## Slide 4: Materials & Sample Preparation
The polymer system studied is SU-8 2002 (SU-8) dissolved in cyclopentanone with poly(ethylene) oxide (PEO) and tetrabutylammonium tetrafluoroborate (TBATFB) as additives.
@campus-MTY
Notes: tetrafluoroborato de tetrabutilamonio

## Slide 5
Sample Preparation @campus-MTY
Sample | PEO concentration | TBATFB concentration
1 | 0.00 wt% | 0.50 wt%
2 | 0.25 wt% | 
3 | 0.50 wt% | 
4 | 0.75 wt% | 
5 | 1.00 wt% | 
During the stirring step, all the samples were isolated from light to avoid any chance of cross-linking of SU-8

## Slide 6: Characterization
Chart: Shear Rate 1/s
| 1.0022400000000001E-2 | 1.25907E-2 | 1.5850300000000001E-2 | 1.9956499999999999E-2 | 2.5115999999999999E-2 | 3.1623800000000001E-2 | 3.98009E-2 | 5.0110399999999999E-2 | 6.3096399999999997E-2 | 7.9435500000000006E-2 | 9.9996100000000004E-2 | 0.125884 | 0.15848799999999999 | 0.19952400000000001
1 | 224.499 | 190.329 | 154.427 | 123.677 | 97.2946 | 76.6557 | 61.9846 | 51.3725 | 41.8653 | 34.9225 | 28.9383 | 24.4038 | 20.6804 | 17.67
0.5 | 200.872 | 171.04 | 130.04 | 100.34 | 78.529 | 61.84 | 49.3856 | 39.566 | 32.2846 | 26.1957 | 21.3532 | 17.5599 | 14.4474 | 11.7366
0.25 | 115.865 | 151.68 | 131.592 | 109.775 | 90.3254 | 73.095 | 58.5037 | 46.9257 | 38.1231 | 31.1414 | 25.2553 | 20.1913 | 16.1194 | 13.0615
0.75 | 46.5633 | 45.411 | 36.6601 | 28.9301 | 22.9455 | 17.5683 | 13.6568 | 11.17 | 8.9524 | 7.482 | 6.0712 | 4.9683 | 4.1105 | 3.4303
0 | 0.32034 | 0.32842 | 0.11051 | 0.07318 | 0.061383 | 0.059807 | 0.047338 | 0.044358 | 0.038571 | 0.035184 | 0.033614 | 0.030545 | 0.029444 | 0.028235

## Slide 7: Characterization
Chart: Shear Rate 1/s
| 5.9848899999999997E-3 | 6.9949299999999999E-3 | 8.1527700000000002E-3 | 9.5058599999999997E-3 | 1.10843E-2 | 1.29251E-2 | 1.5067499999999999E-2 | 1.7579000000000001E-2 | 2.04849E-2 | 2.3887100000000001E-2 | 2.7843900000000001E-2 | 3.00167E-2
1 | 9.2566 | 10.0377 | 9.1425 | 8.4773 | 7.6295 | 6.9489 | 6.7242 | 5.4211 | 4.0774 | 3.9228 | 3.5349 | 3.5236
0.75 | 7.2896 | 7.4373 | 5.8583 | 4.8915 | 4.2151 | 3.5957 | 3.0473 | 2.7302 | 2.3978 | 2.1417 | 1.9055 | 1.7183 | 1.5462 | 1.3626 | 1.2225
0.5 | 1.4217 | 1.3976 | 1.3081 | 1.2134 | 1.1426 | 1.0797 | 1.0105 | 0.94073 | 0.8745 | 0.81988 | 0.77185 | 0.72335 | 0.68 | 0.63933 | 0.60511
0.25 | 0.88151 | 0.96378 | 0.89827 | 0.87306 | 0.86343 | 0.90981 | 0.94664 | 0.96009 | 0.97257 | 0.959 | 0.95349 | 0.99454 | 1.0766 | 1.1591 | 1.2462
0 | 0.31792 | 0.30709 | 0.32546 | 0.32034 | 0.31349 | 0.3018 | 0.28696 | 0.26618 | 0.23766

## Slide 8: Conclusions:
Ensure the samples are properly stirred
Measurements shall not last too long - as the solvent (cyclopentanone) evaporates
Chart: Shear Rate 1/s
| 5.99491E-3 | 6.7304900000000004E-3 | 7.5509100000000001E-3 | 8.4742399999999992E-3 | 9.5083100000000007E-3 | 1.06683E-2 | 1.1972999999999999E-2 | 1.34339E-2 | 1.5076000000000001E-2 | 1.6911700000000002E-2 | 1.8974899999999999E-2 | 2.1287500000000001E-2 | 2.3886399999999999E-2 | 2.67996E-2 | 3.00769E-2 | 3.3733399999999997E-2 | 3.7864599999999998E-2 | 4.24818E-2 | 4.76701E-2 | 5.3474300000000002E-2 | 5.9995800000000002E-2 | 6.7311700000000002E-2 | 7.5518000000000002E-2 | 8.4730200000000006E-2 | 9.5077099999999998E-2 | 9.9982199999999993E-2
Viscosity Pa.s | 1.4217 | 1.3976 | 1.3081 | 1.2134 | 1.1426 | 1.0797 | 1.0105 | 0.94073 | 0.8745 | 0.81988 | 0.77185 | 0.72335 | 0.68 | 0.63933 | 0.60511 | 0.59641 | 0.58965 | 0.5771 | 0.571 | 0.53179 | 0.55319 | 0.63002 | 0.86026 | 1.374 | 2.3386 | 3.7586

## Slide 9: Q&A