## Slide 1: Electrospunable Concentrations
Osamu Katagiri-Tanaka A01212611@itesm.mx
14 Jul 2020

## Slide 2: Agenda
<a point for discussion> : <5min
<another point for discussion> : ~20min

## Slide 3: Let’s focus on polymer concentration
Polymer concentration is the most reliable process parameter to control the morphology of electrospun fibers. (regardless the type of NFES process)

## Slide 4: Let’s focus on polymer concentration
Polymer concentration is the most reliable process parameter to control the morphology of electrospun fibers. (regardless the type of NFES process)

## Slide 5: Literature claims
Under some critical concentration NFES yields beads or small fibres
Over some critical concentration NFES continuous fibres
Viscosity increases with molecular weight
D.R. Flores, Role of rheological properties in near field electrospun fibers morphology, (2017) 130.
G.L. Wilkes, An overview of the basic rheological behavior of polymer fluids with an emphasis on polymer melts, J. Chem. Educ. 58 (1981) 880. https://doi.org/10.1021/ed058p880.
The general belief is that the molecular weight needs to be sufficient enough to create or induce entanglements

## Slide 6: Regarding the previous slide …
N. Bhardwaj, S.C. Kundu, Electrospinning: A fascinating fiber fabrication technique, Biotechnol. Adv. 28 (2010) 325–347. https://doi.org/10.1016/j.biotechadv.2010.01.004.G.L. Wilkes, An overview of the basic rheological behavior of polymer fluids with an emphasis on polymer melts, J. Chem. Educ. 58 (1981) 880. https://doi.org/10.1021/ed058p880.
Hyp.
If chain entanglement is controlled by molecular weight,
increasing molecular weight increases viscosity, and
viscosity is controlled by polymer concentration, then
The critical concentration can be found in a viscosity vs. concentration plot
critical
concentration
?

## Slide 7
successful NFES fibres
POLY(ETHYLENE OXIDE)
SU-8

## Slide 8
POLY(STYRENE-CO-BUTADIENE)
1-METHYL-2-PYRROLIDINONE
successful NFES fibres

## Slide 9
POLYSTYRENE
TETRAHYDROFURAN
successful NFES fibres

## Slide 10
spunable concentrations
non-spunable concentrations
POLY(STYRENE-CO-ALPHA-METHYLSTYRENE)
N,N-DIMETHYLFORMAMIDE

## Slide 12: SU-8

## Slide 13: References
<reference A>
<reference B>

## Slide 14: Title
<content> <key concept>